Supplementary Data for

# Ca-Alginate-Based Janus Capsules with a Pumping Effect for Intestinal-Targeted Controlled Release

Shuang Wen a, Xiao-Jie Ju a,b,*, Wen-Ying Liu a, Yu-Qiong Liu a, Xing-Qun Pu a, Zhuang Liu a,b, Wei Wang a,b, Rui Xie a,b, Yousef Faraj a, Liang-Yin Chu a,b

a School of Chemical Engineering, Sichuan University, Chengdu 610065, China

b State Key Laboratory of Polymer Materials Engineering, Sichuan University, Chengdu 610065, China

* Corresponding author.

E-mail address: juxiaojie@scu.edu.cn (X.J. Ju).

Fig. S1. Schematic illustration of microfluidic preparation for HPMCP microspheres. (a) Preparation of emulsion templates by a microfluidic device. (b) HPMCP microspheres prepared by solvent diffusion.

Fig. S2. Digital photographs and diameter changes of θ-ACPSi capsules in different pH solutions. The scale bar is 5 mm.

Fig. S3. Mechanical properties of θ-AC and θ-ACPSi capsules. (a, b) Digital photographs of (a) deformation and (b) final rupture of θ-ACPSi capsule under extrusion, and the scale bar is 1 cm. (c) The stress–strain curves of extruded θ-AC and θ-ACPSi capsules. (d, e) The stress and strain values of extruded θ-AC and θ-ACPSi capsules.

Fig. S4. The change in drug loading contents of θ-ACPSi capsules stored in 0.2 mol·L−1 acetic acid solution.