Supplementary data for

# Highly Efficient and Precise Rare-Earth Elements Separation and Recycling Process in Molten Salt

Hang Hua a, Kouji Yasuda b, Yutaro Norikawa a, Toshiyuki Nohira a,*

a Institute of Advanced Energy, Kyoto University, Kyoto 611-0011, Japan

b Graduate School of Engineering, Kyoto University, Kyoto 606-8501, Japan

* Corresponding author.

E-mail address: nohira.toshiyuki.8r@kyoto-u.ac.jp (T. Nohira).

The main phases were identified as Mg and MgO, indicating that the evaporated Mg had solidified and a part of the Mg had been oxidized by air exposure. The result indicates that the by-product Mg easily evaporates even at 1123 K without vacuum.

2RE(s, in magnet) + 3MgCl2(l) → 2RECl3(l) + 3Mg(g) 	(1).

In the SEEE process, the evaporated Mg and MgCl2 can be reused together as the RE extraction agent (MgCl2) after the chlorination by Cl2 gas formed in the next step.

Fig. S1. (a) A photo and (b) an XRD pattern for evaporates collected from the low temperature part of the top of container after RE extraction in a molten CaCl2–MgCl2 (3 mol%) system at 1123 K for 20 h without vacuum.

Fig. S2. (a) Cross-sectional SEM image with EDX analysis results and (b) XRD pattern of the sample obtained by the potentiostatic electrolysis with a Ni electrode at a potential of 0.60 V. (c, d) Potential dependences of the (c) RE–Ni alloy formation rate and (d) concentrations of RE elements and Dy:Nd ratio in the RE–Ni alloys. The samples were obtained by the potentiostatic electrolysis with Ni electrodes at various potentials and temperature of 1123 K for 30 min in a molten CaCl2–CaF2 (6.00 mol%)–NdCl3 (2.00 mol%)–DyCl3 (1.00 mol%) system.