Supplementary file for

Controllable Histotomy Based on Hierarchical Magnetic Microneedle Array Robots

Xiaoxuan Zhang a, Hanxu Chen b, Taiyu Song a, Jinglin Wang a, Yuanjin Zhao a,b,*

a Department of Rheumatology and Immunology, Nanjing Drum Tower Hospital, School of Biological Science and Medical Engineering, Southeast University, Nanjing 210096, China

b Oujiang Laboratory (Zhejiang Lab for Regenerative Medicine, Vision and Brain Health), Wenzhou Institute, University of Chinese Academy of Sciences, Wenzhou 325001, China

*Corresponding author.

E-mail address: yjzhao@seu.edu.cn (Y. Zhao).

Fig. S1. (a) Schematic illustration of fabricating the negative template. (b) Digital images of the 3D printed mold, the replicated negative template, and the replicated hydrogel microneedle scaffold. Scale bars: 250 µm.

Fig. S2. Digital images of Ecoflex silicone during stretching. Stretching percentage: (a) 0%, (b) 50%, (c) 100%, (d) 175%. Scale bar: 1 cm.

Fig. S3. (a) Height distribution and (b) diameter distribution of each layer of the microneedle scaffold. n = 230.

Fig. S4. (a) Curing time under UV irradiation and (b) the maximum response distance to external magnets of the magnetic microneedle scaffold materials containing different concentrations of magnetic particles.

Fig. S5. The maximum response distance to external magnets of one single magnetic microneedle fragment, one magnetic microneedle fragment carrying an agarose block, a 2 × 2 magnetic microneedle fragment array carrying an agarose block, and a 3 × 3 magnetic microneedle fragment array carrying an agarose block.

.

Fig. S6. (a) SEM image and (b) H&E staining image of the mouse tumor tissue penetrated by the microneedle. Scale bars: 100 µm.

Fig. S7. Mechanical force tests. (a) Forces detected by a sensor when the multilayered or smooth microneedle scaffolds are pulled out from the mouse tumor tissues. Each type of the microneedle scaffold is tested on three parallel tumor tissues. (b) The maximum force recorded by the sensor during the pulling process.

Fig. S8. Digital image of the components of the microtomy device. Scale bar: 1 cm.

Movie S1. Biohybrid microrobots moving along a line, following a circle, or revolving collectively under the guidance of external magnetic fields.

Fig. S9. Cyto-compatibility of magnetic microneedle scaffold materials. Fluorescence images of tumor cells cultured (a) without materials, (b) with hydrogel microneedle scaffolds, and (c) with magnetic microneedle scaffolds on day 5. Living cells are dyed with Calcein-AM. (d) Corresponding cell viability on days 1, 3, and 5 calculated by MTT assay. The cell viability from the control group on day 1 is set as the baseline. MP: magnetic particle. Scale bars: 100 µm.

Fig. S10. Structure of the microfluidic chip. (a) General design of the microfluidic chip, including four inputs and fifteen outputs for fifteen drug combinations (each with four parallel chambers). (b) Enlarged diagram of fluid input, mixture, branching, convergence, and output of a three-pass chamber.

Fig. S11. Optical images of the seven layers which pile up and bond to one another to constitute the microfluidic chip, as well as the assembled microfluidic chip. L1–5: layer 1–5. Scale bar: 2 cm.

Fig. S12. Numerical simulation of velocity streamline formed in the incubation chamber and fluid intersection at different crossings.

Fig. S13. Positive area ratio of MUC1, EGFR, and Ki67 of fresh tumor tissues acquired from nude mice and sliced tumor tissues cultured in vitro.

1. Supplementary methods

Characterization of the microneedle scaffold: Optical images of the microneedle scaffold were taken by a CCD camera (Oplenic Digital Camera, China) attached to a stereomicroscope (JSZ6S, Jiangnan Novel Optics, China). For colorful display, fluorescent molecules (FITC-BSA, Bersee Co. Ltd, China) were added to the microneedles and the fluorescence images were taken by an inverted fluorescence microscope (CKX41, Olympus, Japan) equipped with a CCD camera (Oplenic Digital Camera, China). The scanning electron microscope (SEM) images and energy dispersive spectrum (EDS) analysis were obtained from a scanning electron microscope (JSM-IT200, JEOL, Japan).

Tumor tissue acquisition from nude mice: Nude mice were anesthetized by inhalation of isoflurane. 200 µL cell suspension of cancer cells (1×108 cells/mL) in 1:1 culture medium : matrigel was injected into their axilla. Noted that the cell suspension should be used as soon as it was prepared and could only be reserved on ice for a little while. The nude mice were raised in SPF environments for 2 weeks. Tumor tissues were cut from the mice after they were sacrificed. The detailed information about the experiment animal and the tumor specimen was listed in Table S1.

Table S1

Information about the experiment animal and tumor specimen.

| Animal | Number | Age | Weight | Modelling method | Harvested tumor volume |
| --- | --- | --- | --- | --- | --- |
| Balb/c nude mice | 12 | 6–8 weeks | 20–25 g | Axilla injection of FG pancreatic carcinoma cells | 200–300 mm3 |

Mechanical tests: The pulling force was measured via a force testing platform (BAB-5MT, Shenzhen Suns Technology Stock Co. Ltd, China). In the beginning, the microneedle scaffold with its needles pointing down was glued on the upper plate of the platform and a piece of mouse tumor tissue was fixed on the bottom plate. The upper plate then moved downward until the microneedle scaffold completely penetrated through the tumor tissue. After that, the upper plate moved upward at the speed of 2 mm/min to pull the microneedle scaffold out from the tumor tissue and the pulling force was recorded by an attached sensor in real time.

Cytocompatibility of the microneedle materials: NCI-H1975 cells were cultured in 24-well plates and randomly divided into three groups. For the control group, cells were cultured in complete culture medium; for the hydrogel group, cells were co-cultured with a solidified polymer block composed of 50% (v/v) PEGDA, 20% (v/v) PEG and 1% (v/v) HMPP; for the hydrogel+MP group, cells were co-cultured with the polymer block of 50% (v/v) PEGDA, 20% (v/v) PEG, 1% (v/v) HMPP and 100 mg/mL NdFeB particles. On day 5, the cells were dyed with Calcein AM and observed under an inverted fluorescence microscope (CKX41, Olympus, Japan). On days 1, 3 and 5, MTT assay was conducted as previously reported [1]. The OD values at 570 nm were by a microplate reader (SynergyHTX, BioTek, USA). The cell viability was calculated based on the OD values.

Numerical simulation: COMSOL Multiphysics [2,3] was employed to simulate fluid flow in the incubation chamber as well as fluid mixture in the microfluidic channels. The numerical simulation was based on Navier-Stokes equation:

ρ∂φ∂τ+ρφ∙∇φ=∇∙-pI+K+F

ρ∇∙φ=0

K=μ∇φ+∇φT

where ρ is the fluid density, φ is the fluid velocity vector, τ is the time, p is the pressure, I is the unit dyadic, F is the volume force vector, μ is the kinetic viscosity of the fluid, and T is the absolute temperature.

References

[1]	Zhang XX, Chen GP, Liu YX, Sun LY, Sun LY, Zhao YJ. Black phosphorus-loaded separable microneedles as responsive oxygen delivery carriers for wound healing. ACS Nano 2020;14(5):5901–8.

[2]	Meng KY, Xiao X, Liu ZX, Shen S, Tat T, Wang ZH, et al. Kirigami-inspired pressure sensors for wearable dynamic cardiovascular monitoring. Adv Mater 2022;34(36):2202478.

[3]	Chen HX, Bian FK, Sun LY, Zhang DG, Shang LR, Zhao YJ. Hierarchically molecular imprinted porous particles for biomimetic kidney cleaning. Adv Mater 2020;32(52):2005394.