Supporting information

Ionically imprinting-based copper (II) label-free detection for preventing hearing loss

Huan Wanga,c,#,*, Hui Zhangb,#, Xiaoli Zhangd, Hong Chend, Ling Lud,*, Renjie Chaib,e,f,g,h,*

a The Eighth Affiliated Hospital, Sun Yat-Sen University, Shenzhen 518033, China

b State Key Laboratory of Digital Medical Engineering, Department of Otolaryngology Head and Neck Surgery, Zhongda Hospital & Advanced Institute for Life and Health, Southeast University, Nanjing 210096, China

c Guangdong Key Laboratory for Biomedical Measurements and Ultrasound Imaging, Department of Biomedical Engineering, Shenzhen University, Shenzhen 518060, China

d Department of Otolaryngology Head and Neck Surgery, Jiangsu Provincial Key Medical Discipline, Nanjing Drum Tower Hospital, The Affiliated Hospital of Nanjing University Medical School, Nanjing 210008, China

e Co-Innovation Center of Neuroregeneration, Nantong University, Nantong 226001, China

f Department of Otolaryngology Head and Neck Surgery, Sichuan Provincial People's Hospital, University of Electronic Science and Technology of China, Chengdu 610072, China

g Institute for Stem Cell and Regeneration, Chinese Academy of Science, Beijing 100101, China

h Beijing Key Laboratory of Neural Regeneration and Repair, Capital Medical University, Beijing 100069, China

# These authors contributed equally to this work.

* Corresponding authors.

E-mail addresses: wangh679@mail.sysu.edu.cn (H. Wang), entluling60@126.com (L. Lu), renjiec@seu.edu.cn (R. Chai)

Fig. S1. The diameter distribution of SCCBs.

Fig. S2. SEM characterization of the composite and collapsed IIHBs. (a) The inside of a composite bead. (b) The surface of a collapsed IIHB. Scale bars are 1 μm in a and 500 nm in b.

Fig. S3. Optical characterization of the green SCCBs. The optical images of (a) SCCBs with green color, (b) the corresponding composited beads and (c) IIHBs. (d) The corresponding reflective wavelength of the beads in (a–c). Scale bars are 200 μm in (a–c).

Fig. S4. Optical characterization of the crimson SCCBs. The optical images of (a) SCCBs with crimson color, (b) the corresponding composited beads, and (c) IIHBs. (d) The corresponding reflective wavelength of the beads in (a–c). Scale bars are 200 μm in (a–c).

Fig. S5. Absorbance detection. (a) The absorbance of ammonia buffer solution, ammonia buffer solution containing DDTC·Na, and ammonia buffer solution containing DDTC·Na and Cu2+. (b) The absorbance of the solution containing different concentrations of Cu2+.

Fig. S6. Standard relation of Cu2+ concentration and the shift value.

Table S1

Cu2+ adsorption capability of IIHBs and NIHBs.

| Bead tpye | Before adsorption (μmol∙L-1) | After adsorption (μmol∙L-1) | Adsorption (μmol∙L-1) | Imprinting factor |
| --- | --- | --- | --- | --- |
| IIHBs | 100 | 26.52 | 73.48 | 19.14 |
| NIHBs | 100 | 96.16 | 3.84 |  |