Supplementary data for

Turning Waste into Valuable Products: Sunlight-Driven Hydrogen from Polystyrene via Porous Tungsten Oxide Photoanodes

Love Kumar Dhandolea, Jun-Tae Kima, Hyoung-il Kimb, Sang Hoon Kima,c,d, Ji-Young Kim,e Jonghun Limf* and Gun-hee Moona,c*

a Extreme Materials Research Center & Climate and Environmental Research Institute, Korea Institute of Science and Technology (KIST), Seoul 02792, Republic of Korea

b School of Civil & Environmental Engineering, Yonsei University, Seoul 03722, Republic of Korea

c Division of Nano & Information Technology, University of Science and Technology (UST), Daejeon 34113, Republic of Korea

d KHU-KIST Department of Converging Science and Technology, Kyung Hee University, Seoul 02447, Republic of Korea

e Advanced Analysis Center, Korea Institute of Science and Technology (KIST), Seoul 02792, Korea.

f Department of Environment and Energy Engineering, Sungshin Women’s University, Seoul 01133, Republic of Korea

* Corresponding authors

E-mail addresses: jlim@sungshin.ac.kr (J. Lim), catalysis@kist.re.kr (G. Moon)

* Corresponding authors: catalysis@kist.re.kr (G. Moon), jlim@sungshin.ac.kr (J. Lim)

Fig. S1. (a) TEM image, (b) HR-TEM (inset SAED) and (c) elemental mapping images of WO3 photoanode.

Fig. S2. Tauc-plot obtained from diffuse reflectance absorption spectra of bare WO3 photoanode.

Fig. S3. Mott–Schottky plots of WO3.

Fig. S4. The water oxidation mechanism on transition metal oxides involves single-metal sites and dual metal-oxo entities.

Fig. S5. PEC transient-chronoamperometry (a) chopped and (b) steady state curves of WO3 photoanode prepared at various anodization potentials.

Fig. S6. 1H NMR spectra of PS commercial (purchased from Sigma Aldrich) and PS plastic foam obtain from packaging waste without further purification.

Fig. S7. Raman spectrum of WO3-PS photoanode demonstrating distinguishable peaks of polystyrene.

Fig. S8. CA curve of WO3-PS collected at 1 VAg/AgCl in the dark.

Fig. S9. Reflectance spectra and photographs of WO3, WO3-PS and WO3-PS-A photoanodes.

Fig. S10. FE-SEM image, EDX spectra and elemental quantification table of (a) WO3, (b) WO3-PS and (c) WO3-PS-A photoanodes.

Fig. S11. TEM-EDS spectrum focused on the TEM image and elemental quantification table of (a) WO3 and (b) WO3-PS-A photoanodes.

Fig. S12. (a) Time-dependent Raman spectra of the WO3-PS system and (b) corresponding relative intensity ratio of WO3 to PS.

Fig. S13. 1H NMR spectra (CDCl3, TMS) of PS plastic foam, electrolyte (HClO4) before and after reaction.

Fig. S14. Images depicting: (a) PS oxidation during the PEC process, and (b) the electrolyte sampled post-reaction, showing PS flakes and peeled-off film.

Fig. S15. 1H NMR spectra (CDCl3, TMS) of PS plastic foam, electrolyte (HClO4) before and after reaction.

Fig. S16. GC-MS spectra of the electrolyte, captured at (a) 1, (b) 2 and (c) 3 hours under illumination. Signals attributed to impurities present in the fresh electrolyte were systematically excluded from all spectra to ensure clarity and focus on the compounds of interest generated or altered due to the PEC oxidation process.

Fig. S17. Proposed mechanism for the photodegradation of PS mediated through the action of photogenerated holes and hydroxyl radicals. This schematic representation elucidates the sequential steps initiated by the absorption of photons by the photoanode, leading to the generation of charge carriers. The photogenerated holes directly participate in the oxidation of PS, while hydroxyl radicals further contribute to the breakdown of the PS polymer chain.

Fig. S18. PEC Transient-CA curves of WO3/FTO.

Fig. S19.  Recycling stability of the WO3 photoanode. After each test, the electrode was cleaned with chloroform and freshly deposited with PS.

Table S1. Raman peaks of PS in WO3-PS photoanode.

| PS bands cm-1 | assignments |
| --- | --- |
| 621.6 | Ring deformation mode |
| 1001.0 | Ring breathing |
| 1031.3 | In-plane CH deformation |
| 1153.5 | C-C stretch |
| 1445.0 | CH2 scissoring |
| 1581.8 | C=C stretch |
| 1601.4 | Ring-skeletal stretches |
| 2846.3 | Ring stretch |
| 2901.7 | Anti-symmetric CH2 stretch |
| 3050.1 | Aromatic CH stretch |

Table S2. IR peaks of PS in WO3-PS photoanode.

| PS bands cm-1 | assignments |
| --- | --- |
| 930 | C-H vibrational bending out-of-plane of the benzene ring |
| 1026 | C-O bond |
| 1450-1600 | C=C bond stretching vibration of the benzene ring |
| 2850 | Symmetrical stretching vibration of CH2 bonds |
| 2920 | Asymmetrical stretching vibration of CH2 bonds |
| 3000-3100 | =C-H stretching of the aromatic ring |

Table S3. EIS fitted equivalent circuit model and determined fitted values of circuit components of WO3, WO3-PS and WO3-PS-A.