Supplementary data for
Conversion Mechanism of Biomass to Nano Zero-Valent Iron Biochar: Iron Phase Transfer and In situ Reduction

Sheng-Nan Zhuo, Hong-Yu Ren*, Guo-Jun Xie, De-Feng Xing, Bing-Feng Liu*
State Key Laboratory of Urban Water Resource and Environment, School of Environment, Harbin Institute of Technology, Harbin 150090, China

*Corresponding authors:

E-mail addresses: rhy@hit.edu.cn (H.-Y. Ren), lbf@hit.edu.cn (B.-F. Liu).
[image: image13.png]— 55.68%

—4177% PFI00BC _
b sp*-C o 2172%

PEC— o 32.94% (700°C) ~

PFROBC 2
(700 °C)

Intensity (a.u.)

sp>-C
= C-0.
= }
&
2
PF80BC z PF100BC 3631
(500°C) o e 2 (500°C) 1250,
$p-C —38.19% spC
e
sp-C sp*-C-
C-O0 c=0. CO._

T T T T T T T T T T
292 290 288 286 284 282 280 292 290 288 286 284 282 280

Binding Energy (eV) Binding Energy (eV)




Fig. S1 Illustration of strategy for preparation of nZVI-BC. 

[image: image2]
Fig. S2 (a) SEM image of BC; (b) XPS analysis of BC, (c) SEM image of PF80BC.
Table S1 

Element atomic content (%) on the surface of biochar by XPS

	Sample
	Fe 2p
	O 1s
	C 1s

	BC

FBC

PF80BC

PF100BC
	0.39

0.39

0.77

0.93
	10.8

11.87

10.01

7.87
	88.81

87.73

89.23

91.2


Table S2 

Textural parameters of as-prepared BC, FBC and nZVI-BC.
	Sample
	SBET (m2/g)
	Dp

(nm)
	Vtot (m3/g)
	Vmicro

(m3/g)
	Vmecro

(m3/g)
	Vmicro/ Vtot (%)

	BC

FBC

PF60BC

PF80BC

PF100BC
	136.164

290.613

301.045

320.732

373.079
	3.23

2.21

2.27

2.228

2.16
	0.11

0.161

0.1714

0.1787

0.2015
	0
0.101

0.108

0.128

0.15
	0.11

0.038

0.0634

0.0507

0.0515
	0
62.73

63.01

71.62

74.44


SBET: BET surface areas; Dp: Average pore diameter; Vtot: Total pore volume; Vmicro: Micropore volume; Vmecro: Mesopore volume; Vmicro/ Vtot : The ratio of Vmicro to Vtot.
[image: image1.png]Rice straw

. ° ¢ .
i
PEG | |FeCl, o .
S ¢ - - —
. O X o N () Rl
Washed and Dried Magnetic
700°C Carbonization 2h nZVI-Biochar

Oil bath 0.5h  Rice Straw



 Fig. S3 (a) Zeta potential of as-prepared PF100BC under different pH, (b) XRD spectra of PF100BC under different time.
[image: image3.png]90

BC

10

('ne) Aysusyu|

26 (degree)




Fig. S4 XRD spectrum of BC.
[image: image5.png]o)




[image: image6.emf]3500 3000 2500 2000 1500 1000 500

 

Wavenumbers (cm

-1

)

 

 

Transmittance (a.u.)

 PF-RS

 F-RS

 RS


Fig. S5 The pictures of modified RS under different conditions: (a) RS; (b) F-RS; (c) PF80-RS; (d) PF100-RS.
Fig. S6 FTIR spectra of RS, F-RS and PF80-RS
Table S3 

Element atomic content (%) on the surface of biochar by XPS

	Sample
	Fe 2p
	O 1s
	C 1s

	RS

F-RS

PF80-RS

PF100-RS
	0.14

0.32

3.33

5.47
	21.18

21.76

28.72

28.36
	78.68

77.92

67.95

66.17


Table S4 
Assignments of FTIR spectra of PFx-RS

	Wavenumbers (cm-1)
	Assignments

	2919
	C-H stretching

	1732
	C=O ester; carbonyl groups in branched hemicellulose

	1513
	Aromatic skeletal vibration

	1384
	C-H stretching of cellulose

	1245
	C-O stretching

	1163
	C-O-C asymmetrical stretching

	1061
	C-O stretching of cellulose and hemicellulose

	898
	C-O-C stretching of cellulose


[image: image7.jpg]


Fig. S7 XRD spectra of PF80BC and PF100BC under the pyrolysis of 500 °C.
[image: image8.jpg]



Fig. S8 High-resolution C1s XPS of (a) PF80BC and (b) PF100BC under the pyrolysis of 500 °C and 700 °C.
Table S5 
Element atomic content (%) on the surface of biochar by XPS 

	Sample
	Fe 2p
	O 1s
	C 1s
	O/C

	PF80BC (500 °C)

PF100BC (500 °C)

PF80BC (700 °C)

PF100BC (700 °C)
	1.66

1.48

0.77

0.93
	10.58

11.78

10.01

7.87
	87.76

86.74

89.23

91.2
	0.12

0.13

0.11

0.086


[image: image4.emf]0 50 100 150

0

4

8

12

16

20

24

28

 

 

C

t (mg/l)

Time (min)

Ct Ct k k Statistics Statistics

Value Standard E

rror

Value Standard E

rror

Reduced C

hi-Sqr

 R2

26.49531 0.58483 0.37604 0.08016 2.35088 0.97012

C

t

=26.495(1-e

-0.376t

)


Fig. S9 Experimental and modelling results of CR removal by PF100BC catalysis. Experimental conditions: CR (30 mg/l), PF100BC (0.5 g/l), PS (1.8 mmol/l), T (30 °C).
According to our experimental data, the removed CR concentration can be expressed by the empirical equation:

Ct = Cultimate (1-exp(−kt ))

Where Ct is the removed CR concentration at reaction time t, Cultimate is the ultimate removed CR concentration, k denotes the empirical rate constant(min−1). 
d





c





a





b








[image: image9.jpg]


[image: image10.jpg]


[image: image11.emf]20 30 40 50 60 70 80

 

PF100BC(500℃)

 

PF80BC(500℃)

2θ (degree)

 

[image: image12.png]Zeta potential (mV)

PHpze

o
IS

240 days

0 day

20

30 40

50 60
26 (Degree)

70

80




