# Molecular Simulation of Cement-based Materials and Their Properties: A Review

Ashraf A. Bahraq1, Mohammed A. Al-Osta1, 2, Omar S. Baghabra Al-Amoudi1, 2, I. B. Obot2, Mohammed Maslehuddin2, Habib-ur-Rehman Ahmed1, and Tawfik A. Saleh 4,3 *

1 Department of Civil and Environmental Engineering, King Fahd University of Petroleum & Minerals, Dhahran 31261, Saudi Arabia

2 Interdisciplinary Research Center for Construction and Building Materials
3 Interdisciplinary Research Center for Advanced Materials, King Fahd University of Petroleum and Minerals, Dhahran 31261, Saudi Arabia

4 Department of Chemistry, King Fahd University of Petroleum and Minerals, Dhahran 31261, Saudi Arabia

*Correspondence to: E-mail address:  tawfik@kfupm.edu.sa

Figure S1 Key steps in a molecular dynamics cycle.

Figure S2 Schematic illustration of the bonded and non-bonded interactions in the potential force field systems [29].

Table S1 Force fields commonly used in modeling cementitious systems.

| Force field* | Background | Applications in cementitious materials |
| --- | --- | --- |
| COMPASS | It was originally developed for covalent molecules (e.g., polymer, organic, and small inorganic molecules). It has complicated cross-terms, including valence and non-bonded interaction terms (for the van der Waals term and a Coulombic function) [30]. Generally, it is a high-quality ab initio force field. | Hydrated cement phases [31]–[33]. Silicate phases (C3S and C2S) [31]. Alumino-silicates [34]. Chemical admixtures [20], [35], [36]. |
| ClayFF | It was developed for mineral/water interfaces (mostly for clay-related phases). It treats most inter-atomic interactions as being non-bonded [37]. | Hydrated cement phases [38]. Cement-polymer interaction [39]. Cement-water interaction [40]. Geopolymer-ions interaction [41], [42]. Hydrated crystalline compounds interaction with liquid phases [43]. |
| IFF | It was developed for inorganic-organic and inorganic-biomolecular interfaces. It covers all elements of the periodic table [44]. | The initial hydration and cohesive properties of C3S and C3A [45], [46]. Tricalcium aluminate crystals [47]. Ettringite [48]. Chemical admixtures [49]. |
| CSH-FF | This is a modified version of ClayFF. It is specially designed to describe the interaction between atoms in the cement systems [50]–[52]. | Property prediction of C-S-H [50]. Fracture of C-S-H under loading [51]. C-S-H-polymer nanocomposites [53]. |
| CVFF | It is a generalized valence force field that has been parameterized for water, amino acids, free ions and a variety of other functional groups, as well as some inorganic materials, including silica [54], [55]. | Cement-coating interface [56]. Silica-polymer interface [57], [58]. Cement-PVA interaction [59]. Graphene oxide sheet [60], [61]. |
| Universal | It is mainly a diagonal, harmonic force field where electrostatic and van der Waals interactions are described by atomic monopoles and Lennard-Jones potential, respectively. It is applicable to all elements of the periodic table. [31], [62]. | Cement clinker phases [30]. Hydrated cement phases [31]. |
| Dreiding | It is a good robust all-purpose force field. It permits for fair prediction of many numbers of structures [31]. | Hydrated cement phases [31]. |
| PCFF | It is primarily developed for application to polymers and organic materials. It is similar to the COMPASS force field; however, it is parametrized for a range of functional groups [63]. | Chemical admixtures in cement [49]. |
| ReaxFF | It was developed by Duin et al. [64] for applications to catalysis, gas-phase reaction, and material failure. It is the force field that links the quantum mechanics and classical MD simulations. Currently, it is used for chemical simulations of a variety of materials, including metals, ceramics, silicon, and polymers [23], [65]. | Chemical reaction of C-S-H [66], [67]. Polymerization and hydrolytic reactions of C-A-S-H [68]. Rebar passivation in concrete [23]. Polymers [69]. |
| - *COMPASS = Condensed-phase Optimized Molecular Potentials for Atomistic Simulation Studies - CVFF = Consistent valence force field - IFF = INTERFACE force field - PCFF = Polymer Consistent Force Field - ReaxFF = Reactive force field |  |  |