# Supplementary data for

Bacteria-photocatalyst biohybrid system for sustainable ammonium production

Meiwei Guo, Guangfei Liu, Sen Qiao *, Xie Quan *

Key Laboratory of Industrial Ecology and Environmental Engineering (Ministry of Education, China), School of Environmental Science and Technology, Dalian University of Technology, Dalian 116024, China

*Corresponding authors:

E-mail addresses: qscyj@mail.dlut.edu.cn (S. Qiao), quanxie@dlut.edu.cn (X. Quan)

# Text S1. Optimization of Cadmium Concentration

Although cadmium ion (Cd2+) presents high biological toxicity and will cause oxidative damage to cells, some studies had proved that toxic Cd2+ could exist on the cell wall in the form of precipitation, preventing the spread of toxicity [1]. Several researchers have proved that non-photosynthetic bacteria were able to biologically precipitate CdS nanoparticles on the surface of cells and further implement CO2 to acetic acid by M. thermoaccia-CdS biohybrid systems [2], NO3- to N2O by T. denitrificans-CdS biohybrid system [3]. Therefore, the optimal cadmium concentration that S. oneidensis MR-1 could tolerate was explored firstly in our study, mainly based on the optical density values at 600 nm (OD600). As shown in Fig. S1, with the Cd2+ concentration in the range of 0.02 mM-0.2 mM (cysteine as S source, 0.06 mM-0.6 mM), the OD600 of S. oneidensis MR-1 appeared fluctuation compared with the control group (Cd2+=0.0 mM). When the concentration of Cd2+ was 0.10 mM, the OD600 reached the maximum, denoting that 0.10 mM was the optimal concentration of Cd2+ in S. oneidensis MR-1 bacterial suspension to generate CdS precipitation. Therefore, 0.10 mM of Cd2+ was chosen to form S. oneidensis MR-1/CdS biohybrid system.

Text S2. S. oneidensis MR-1/CdS reaction equations

Electron-hole pair photogeneration:

NO3- reduction to NH4+:

NO3-+10H++8e-S.  oneidensis MR-1/CdSNH4++3H2O

Cysteine oxidation to cystine:

2Cys+2h+S.  oneidensis MR-1/CdSCyss+2H+

Overall photosynthetic reaction:

NO3-+2H++8Cys+8hvS.  oneidensis MR-1/CdSNH4++3H2O+4Cyss

Fig. S1. Cell density (OD600) of S. oneidensis MR-1 inoculated with different concentrations of CdCl2. All the results were the average of tri-measurements with standard error.

Fig. S2. SEM image of S. oneidensis MR-1 before biosynthesis.

Fig. S3. UV-Vis spectra of S. oneidensis MR-1/CdS demonstrating a band gap of 2.37 ± 0.05 eV.

Fig. S4. XRD analysis of S. oneidensis MR-1 biosynthesis CdS was consistent with cubic structure (standard card JCPDS card No. 10-0454).

Fig. S5. Changes of nitrogen during photocatalytic degradation of NO3- in (a) S. oneidensis MR-1 △MtrC-△OmcA/CdS biohybrid system and (b) S. oneidensis MR-1 △CymA/CdS biohybrid system. All the results were the average of tri-measurements with standard error.

Table S1 Peptide sequences selection for PRM analysis.

| Entry Name | Gene Names | Peptide Sequence |
| --- | --- | --- |
| Q8EG35 | MtrA, SO_1777 | MTPEQVEATLDK GGNEPMITFGK |
| Q8CVD4 | MtrB, SO_1776 | YANQLNTDAVDAK VDLLGMNLK LGLDYTYSNSDSNTQVR |
| P83223 | FccA, SO_0970 | GEYTGYYVIK ADAVVIAAGGFAK FMNEITTR GESAYLVFDDSIR |
| Q8EAC7 | NrfA, SO_3980 | EFLVGVTNER GLTDPVAIPDISTK AQAVLGMDMEK |
| Q8EIJ1 | NapA, SO_0848 | AGFLTNNIDPNAR LPADMVVDNDK VAEVWPAELIAK LILDATDPLSK |

References

- Wang, B. et al. Enhanced Biological Hydrogen Production from Escherichia coli with Surface Precipitated Cadmium Sulfide Nanoparticles. Adv. Energy Mater. 7, 1-10 (2017).

- Sakimoto, K.K., Wong, A.B., Yang, P.D. Self-photosensitization of nonphotosynthetic bacteria for solar-to-chemical production. Science 351, 74-77 (2016).

- Chen, M. et al. Light-driven nitrous oxide production via autotrophic denitrification by self-photosensitized Thiobacillus denitrificans. Environ. Int. 127, 353-360 (2019).