Supplementary data for

The Low-Attenuation Endfire Leaky-Wave State on an Optically Transparent Lossy Film

Ziheng Zhoua, b, Yongjian Zhangb, Yilin Zhengc, Ke Chend, Yueming Gaoa, Yuehe Gea,

Yue Lib,*, Yijun Fengd,*, Zhizhang (David) Chena, e,*

a College of Physics and Information Engineering, Fuzhou University, Fuzhou 350108, China

b Department of Electronic Engineering, Tsinghua University, Beijing 100084, China

c School of Electronic and Information Engineering, Soochow University, Soochow 215006, China

d School of Electronic Science and Engineering, Nanjing University, Nanjing 210023, China

e Department of Electrical and Computer Engineering, Dalhousie University, Halifax, NS B3H 4R2, Canada

* Corresponding authors.

E-mail addresses: lyee@tsinghua.edu.cn (Y. Li), yjfeng@nju.edu.cn (Y. Feng), z.chen@dal.ca (Z. Chen).

S1. Dispersion equation of the TM1 mode of the TCF-grounded GSW

For a GSW (shown in Fig. 1(a) in the main text) extending along the +y axis, the transverse components of electromagnetic fields under the TM modes exhibit cosinusoidal variation along the +z axis in the glass slab (0 < z < h), while exhibiting exponentially decaying behavior along the +z axis in the air (z > h) [1]. The expressions of field components Ey, Ez, and Hx in the glass slab (0 < z < h) are given by [1]

|  |  | (S1-1) |
| --- | --- | --- |
|  | (S1-2) |  |
|  |  | (S1-3) |

and the expressions of electric and magnetic field components Ey, Ez, and Hx in the air-filled region (z > h) are

|  | (S2-1) |
| --- | --- |
|  | (S2-2) |
|  | (S2-3) |

where A and B are amplitude coefficients, ω is the angular frequency, and εr = 7.3 is the relative permittivity of the glass slab. β denotes the phase constant for the wave propagating toward the +y direction, while T and τ denote the transverse wave numbers in the glass layer and the air-filled space. Since the conductivity of the TCF is significantly larger than that of the glass slab, we have approximately treated the TCF at z = 0 as the perfect electric conductor (PEC) boundary. Imposing the boundary condition that tangential components of fields shall be continuous across the glass-air interface, we obtain the relationship of coefficients A and B as

(S3)

the dispersion equation for the GSW’s TM mode is derived as:

(S4)

where k0 represents the wave number in free space. For the fundamental propagation mode of the GSW, i.e., TM1 mode, its phase constant β is determined by the solution of Eq. (S4) with the smallest transverse wave number T. Once the electromagnetic fields in the GSW structure are solved from Eqs. (S1) and (S2), powers transmitted in the air and glass slab can be evaluated by

(S5)

and

(S6)

and the total transmitted power Ptotal in the TCF-grounded GSW is the sum of Pair and Pslab.

S2. Attenuation constants of the TCF-grounded GSW’s TM1 mode

Here we applied the perturbation method [2] to calculate the attenuation constant αTCF of the TCF-grounded GSW’s TM1 mode due to TCF loss. Assume an exponential decay of the total transmitted power due to TCF loss, i.e., Ptotal(l)  exp(−2αTCFl), where l denotes the propagation distance. The attenuation constant αTCF is related to the total transmitted power Ptotal and ohmic loss per unit length QTCF = 0.5Rs|JTCF|2 via

(S7)

It is noted that the magnitude surface current density JTCF on the TCF equals that of the tangential magnetic field Hx(z = 0). The explicit expression of attenuation coefficient αTCF then can be derived as

(S8)

- For h/λ0 → 0, an asymptotic expression of αT can be obtained as

- (S9)

Next, we derive the expression of attenuation constant αrad due to radiation leakage. Since the power Pair transmitted in the air region would eventually leak into the free space, the attenuation coefficient αrad due to radiation leakage is determined by αrad = ‒12Lln[(Ptotal ‒ Pair) / Ptotal], where an exponential decay of power due to leakage radiation is assumed. Note that the ratio of Pair to Ptotal is evaluated by

(S10)

and an explicit expression of attenuation constant αrad due to radiation leakage is therefore derived as

(S11)

When the normalized glass-slab thickness h/λ0 is sufficiently small, an asymptotic expression of the power distribution ratio is derived from Eq. (S10) as Pair/Ptotal ≈1−2(εr − 1)h2k02/εr, and an approximate expression of αrad can be deduced as

(S12)

S3. Numerical calculation setup

Full-wave simulations of the 3D TCF-grounded GSW structure are performed based on finite-element-method (FEM) simulation software Ansys HFSS® (ANSYS, USA). The 3D domain is discretized into tetrahedral elements, and the adaptive meshing is applied until the variation of the S-parameters is smaller than 0.01. The TCF is modeled by the impedance boundary condition with a specific sheet resistance. To emulate the open space in which the antenna is placed, the perfectly matched layer (PML) boundary is applied at one wavelength away from the GSW structure.

S4. Method to extract attenuation constants attributed to radiation leakage and material absorptions

The total attenuation constant αtotal can be decomposed into those incurred by ohmic loss of TCF, dielectric loss of glass, and radiation leakage; namely, αtotal = αTCF + αglass + αrad. To see the contributions of those three parts, we study two reference cases C1 and C2 with different material settings. In case C1, the glass slab is lossy (with tanδ = 0.008) while the ground is made of the perfect electric conductor (Rs = 0 Ω/sq). In case C2, all the materials are assigned lossless. The total attenuation constant α for the propagation in the TCF-grounded GSW structure with length L is retrieved from the transmission coefficient T and reflection coefficient R via:

(S13)

The extracted attenuation constants αC1 and αC2 for cases C1 and C2 are plotted by using dashed lines in Supplementary Fig. (S1). It is clear to see that αrad = αC2 due to the absence of material losses in case C2. The attenuation constant αTCF caused by the ohmic loss in the TCF equals αtotal − αC1, while the attenuation constant αglass caused by the dielectric loss in the glass slab equals αC1 − αC2.

S5. Theoretical calculation of the antenna’s gain

The calculation of the far-field radiated fields of the transparent antenna (shown in Fig. 3(a)) is based on Green’s function approach. In the theoretical model of the leak-wave antenna as illustrated in Supplementary Fig. 2, the equivalent magnetic current on the aperture is assumed to be uniformly distributed along the x-axis over an effective aperture width of weff while propagating along the y-axis with a complex propagation constant of β − jαtotal (“j” is the imaginary unit), that is

(S14)

The explicit expression of vector potential at the far-field region is obtained by introducing Green’s function in 3D free space:

(S15)

where the effective aperture width weff is chosen as 0.7λ0. The far-field electric field is then derived from the vector potential via

(S16)

where k is the wave vector pointing to the direction given by the elevation angle θ and azimuth angle φ

(S17)

The expression of the far-field electric field is obtained via some mathematical manipulations as

(S18)

To simplify the above expression, we use the fact that the most power has leaked out or been dissipated after traveling a sufficiently large distance L, and we obtain

(S19)

Once the far-field electric field has been evaluated, the distribution of antenna gain over the space can be calculated via its definition

(S20)

where η is the antenna efficiency. The antenna efficiency can be expressed as the product of feeding efficiency ηfeed and radiation efficiency ηrad, and calculated via

(S21)

Here R is the reflection coefficient of the antenna, ηtrans. is the transmission efficiency of the step transitional structure made by the lossy glass and TCF, the ratio of leakage-induced attenuation coefficient αrad to the total attenuation coefficient (αrad + αslab+ αTCF) is the estimated radiation efficiency [3]. It is noted that the complex propagation constant β − jαtotal is dependent on the GSW thickness h. The antenna gain pattern is finally derived as

(S22)

where C(β, αtotal) is the normalization factor associated with the spherical integration of the radiation intensity

(S23)

Because the TCF-grounded GSW operates in the slow-wave region, i.e., β/k0 > 1, it is easy to know from Eq. (S23) that the antenna’s peak gain in space is achieved in the direction of θ = 90° and φ = 90°.

S6. Antenna fabrication and measurement

The prototyped transparent leaky-wave antenna based on the GSW structure was fabricated using glass materials. The radiation structure is made of soda-lime glass with a relative permittivity of 7.3 and a dielectric loss tangent of 0.008 around 8.6 GHz, while the stepped transition is made of quartz glass with a relative permittivity of 3.75 and a loss tangent of 1×10−4 around 8.6 GHz. The ITO film was deposited on the bottom of the soda-lime glass by using the magnetron sputtering technique, which has a thickness of 400 nm. The skin depth of ITO determined by 1/πfμ0σ (μ0 is the permeability of vacuum, the electrical conductivity σ of ITO is 8.3 × 105 S/m, and f is the operating frequency) is about 6 μm at f = 8.6 GHz, which is significantly larger than the thickness t of the ITO film. For the sub-skin-depth conductive film, its sheet resistance Rs is determined by Rs = 1/(σt), and the sheet resistance of the deposited ITO film is therefore 3 Ohm/sq. To excite the antenna, a 50-Ohm SMA connector with 4-mm-length inner probes was installed at a distance of λg/4 (λg is the wavelength in the glass at the operating frequency of 8.6 GHz) away from the end of the waveguide. The reflection coefficient of the antenna was measured with a vector network analyzer Agilent N9917B, while the measurement of the antenna’s far-field radiation characteristics was carried out in a standard microwave anechoic chamber.

S7. More details of wireless image transfer experiment

In the wireless image transfer experiment, the Tx and Rx leaky-wave antennas are separated horizontally by a center-to-center distance Rc of 1.5 m (43λ0 at 8.6 GHz), and the emission power Pe is set as 0.01 mW, i.e., −20 dBm in logarithmic scale. The received power Pr can be determined according to the Friis transmission [4],

(S24)

where Gt and Gr are the Tx and Rx antenna gains in the transmission direction while Lt (or Lr) denotes the attenuation of the Tx (or Rx) path due to the cables and mixers. Since the operating wavelength λ0 (= 34.88 mm) as well as path losses Lt (measured as 0.063, i.e., −12 dB) and Lr (measured as 0.08, i.e., −11 dB) are fixed, the received power, namely the received signal strength, is solely related to the gains of Tx and Rx antennas. The higher the antenna gains are, the better the wireless transmission quality would be expected.

Fig. S1. Extracted attenuation constants at f0 = 8.6 GHz for various material property settings. αtotal is the total attenuation coefficient of the leaky-wave structure composed of lossy a TCF ground and a lossy glass slab, αC1 corresponds to the leaky-wave structure composed of a perfect electric conductor (PEC) ground and a lossy glass slab, and αC2 corresponds to the leaky-wave structure composed of a PEC ground and a lossless glass slab.

Fig. S2. Illustration of the theoretical model for calculating the leak-wave antenna’s gain. We assume the equivalent magnetic current is distributed according to M(x, y) = M0·exp[(−jβ − αtotal)y]x over a two-dimensional region defined by −weff /2 <  x < weff /2 and 0 < y < L.

Fig. S3. Characterization of the feeding horn antenna. (a) The structure, (b) simulated 3D realized-gain pattern (at 8.6 GHz), and (c) simulated reflection coefficient of the feeding horn. (d) Total efficiencies of the feeding horn and the GSW-loaded antenna. (e) Realized gain and directivity of the feeding horn compared to the measured realized gain of the GSW-loaded antenna.

Fig. S4. Impact of structural width on the antenna performance. (a) Top view of the proposed leaky-wave antenna. Radiation patterns of the antenna on the x-y plane at 8.6 GHz with (b) w1 = 42 mm fixed yet w varying and with (c) w = 66 mm fixed yet w1 varying. (d) and (e) are electric-field magnitude distributions corresponding to cases in (b) and (c), respectively.

Fig. S5. Antenna far field measurement setup

Fig. S6.  Radiation pattern of the proposed transparent leaky-wave antenna. Measured and simulated angular distributions of the antenna gain at f0 = 8.6 GHz on the y-z and x-y cut-planes. Co-pol: co-polarization gain; X-pol: cross-polarization gain.

Fig. S7. Measured and simulated radiation efficiencies of the proposed transparent antenna. The radiation efficiency is defined by the ratio of the radiated power to the power sent into the antenna.

Fig. S8. Power distribution analysis. (a) Simulated scattering parameters of the two-port TCF-grounded GSW and (b) power distribution at 8.6 GHz. (c) Reflection coefficients of the one-port TCF-grounded GSW and (d) power distribution at 8.6 GHz.

Fig. S9. Impact of ITO sheet resistance on antenna performance. Simulated results of (a) peak realized gain and (b) radiation efficiency of the proposed optically transparent leaky-wave antenna using ITO film with various sheet resistances.

Fig. S10.  Photograph of the opaque metal-based endfire leak-wave antenna. The antenna consists of a soda-lime glass slab with a thickness of 1.82 mm (0.052λ0) and an area of 276 mm × 66 mm (7.9λ0 × 1.9λ0). A copper sheet with an area of 7.9λ0 × 1.2λ0 and sheet resistance Rs = 0.025 Ohm/sq is attached to the back of the glass slab.

Fig. S11. Constellation Diagrams of QPSK modulation for the different Rx/Tx antenna settings. (a)-(d) are respectively four constellation diagrams of received signals after wireless transmission using proposed and reference antennas Ant.0-Ant.3. In the constellation diagram, “I” means the in-phase component, and “Q” means the quadrature component. A higher signal-to-noise level manifests as a more concentrated distribution of sampling points.

References

- Pozar DM. Microwave engineering, 4th ed, chapter 3. Hoboken: NJ, USA: John Wiley & Sons, 2011.

- Collin RE. Field theory of guided waves, 2nd ed, chapter 4. Piscataway: NJ, USA: IEEE Press, 1991.

- Liu J, Jackson DR, Li Y, Zhang C, Long Y. Investigations of SIW leaky-wave antenna for endfire-radiation with narrow beam and sidelobe suppression. IEEE Trans Antennas Propag 2014; 62:4489–4497.

- Bertoni HL, Radio propagation for modern wireless systems. Upper Saddle River: NJ, USA: Prentice-Hall, 2000.