Supplementary Data for

# A Multi-Scale Graph Neural Network for the Prediction of Multi-Component Gas Adsorption

Lujun Li a,b,c, Haibin Yu b,c,*

a Department of Automation, University of Science and Technology of China, Hefei 230026, China

b State Key Laboratory of Robotics, Shenyang Institute of Automation, Chinese Academy of Sciences, Shenyang 110016, China

c Key Laboratory of Networked Control Systems, Chinese Academy of Sciences, Shenyang 110016, China

* Corresponding author.

E-mail address: yhb@sia.cn (H. Yu).

S1. Parameters for the force fields used in this paper

Table S1

parameters for the UFF force fields used in this work.

| Element | σ (Å) | ε/kB (K) | Element | σ (Å) | ε/kB (K) | Element | σ (Å) | ε/kB (K) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H | 2.571 | 22.156 | Kr | 3.689 | 110.782 | Lu | 3.243 | 20.646 |
| He | 2.104 | 28.199 | Rb | 3.665 | 20.142 | Hf | 2.798 | 36.255 |
| Li | 2.184 | 12.589 | Sr | 3.244 | 118.336 | Ta | 2.824 | 40.788 |
| Be | 2.446 | 42.802 | Y | 2.980 | 36.256 | W | 2.734 | 33.738 |
| B | 3.638 | 90.640 | Zr | 2.783 | 34.745 | Re | 2.632 | 33.235 |
| C | 3.431 | 52.873 | Nb | 2.820 | 29.710 | Os | 2.780 | 18.632 |
| N | 3.261 | 34.745 | Mo | 2.719 | 28.199 | Ir | 2.530 | 36.736 |
| O | 3.118 | 30.213 | Tc | 2.671 | 24.171 | Pt | 2.454 | 40.284 |
| F | 2.997 | 25.178 | Ru | 2.640 | 28.199 | Au | 2.934 | 19.639 |
| Ne | 2.889 | 21.149 | Rh | 2.609 | 26.688 | Hg | 2.410 | 193.869 |
| Na | 2.658 | 15.107 | Pd | 2.583 | 24.171 | Tl | 3.873 | 342.418 |
| Mg | 2.691 | 55.895 | Ag | 2.805 | 18.128 | Pb | 3.828 | 333.857 |
| Al | 4.008 | 254.296 | Cd | 2.537 | 114.811 | Bi | 3.893 | 260.842 |
| Si | 3.826 | 202.429 | In | 3.976 | 301.630 | Po | 4.195 | 163.656 |
| P | 3.695 | 153.585 | Sn | 3.913 | 285.516 | At | 4.232 | 143.010 |
| S | 3.595 | 137.974 | Sb | 3.938 | 226.097 | Rn | 4.245 | 124.882 |
| Cl | 3.516 | 114.307 | Te | 3.982 | 200.415 | Fr | 4.365 | 25.178 |
| Ar | 3.446 | 93.158 | I | 4.009 | 170.705 | Ra | 3.276 | 203.437 |
| K | 3.396 | 17.624 | Xe | 3.924 | 167.381 | Ac | 3.099 | 16.617 |
| Ca | 3.028 | 119.846 | Cs | 4.024 | 22.660 | Th | 3.025 | 13.092 |
| Sc | 2.936 | 9.568 | Ba | 3.299 | 183.294 | Pa | 3.050 | 11.078 |
| Ti | 2.829 | 8.560 | La | 3.138 | 8.560 | U | 3.025 | 11.078 |
| V | 2.801 | 8.057 | Ce | 3.168 | 6.546 | Np | 3.050 | 9.568 |
| Cr | 2.693 | 7.553 | Pr | 3.213 | 5.036 | Pu | 3.050 | 8.057 |
| Mn | 2.638 | 6.546 | Nd | 3.185 | 5.036 | Am | 3.012 | 7.050 |
| Fe | 2.594 | 6.546 | Pm | 3.160 | 4.532 | Cm | 2.963 | 6.546 |
| Co | 2.559 | 7.050 | Sm | 3.136 | 4.028 | Bk | 2.975 | 6.546 |
| Ni | 2.525 | 7.553 | Eu | 3.112 | 4.028 | Cf | 2.952 | 6.546 |
| Cu | 3.114 | 2.518 | Gd | 3.001 | 4.532 | Es | 2.939 | 6.043 |
| Zn | 2.462 | 62.441 | Tb | 3.074 | 3.525 | Fm | 2.927 | 6.043 |
| Ga | 3.905 | 208.976 | Dy | 3.054 | 3.525 | Md | 2.917 | 5.539 |
| Ge | 3.813 | 190.848 | Ho | 3.037 | 3.525 | No | 2.894 | 5.539 |
| As | 3.769 | 155.599 | Er | 3.021 | 3.525 | Lw | 2.883 | 5.539 |
| Se | 3.746 | 146.535 | Tm | 3.006 | 3.021 |  |  |  |
| Br | 3.732 | 126.392 | Yb | 2.989 | 114.811 |  |  |  |

Table S2

Lennard–Jones parameters for the TraPPE force fields used in this paper.

| Element | σ (Å) | ε/kB (K) |
| --- | --- | --- |
| C (in CO2) | 2.745 | 29.933 |
| O (in CH4) | 3.017 | 85.671 |
| N (in N2) | 3.306 | 38.299 |

S2. Proofs of periodic invariance.

Notations. We use (A,P,L) to describe a given MOF structure. A=[α1,α2,…,αn]T∈Rn×da is the atom feature matrix, where αi∈Rda is the da-dimensional feature vector for atom i in the unit cell. P=[p1,p2,…,pn]T∈Rn×3 is the position matric, where pi∈R3 is the 3D cartesian coordinates for atom i. L=[l1,l2,l3]T∈R3×3. In this way, the infinite MOF structure can be represented as P={pi|pi=pi+k1l1+k2l2+k3l3,  k1, k2,k3∈Z,i∈Z, 1≤i≤n}, and A={ai|ai=ai,  i∈Z, 1≤i≤n}. P describes all positions for each atom i, A described the atom feature for each atom i. L representing the minimum repeating patterns is given. When L representing the minimum repeating patterns is given, the periodic invariance lies in the invariance to shifts of periodic boundaries. We demonstrate that the multi-edge graph construction of the crystal used in our MHACGNN-MS satisfies the periodic invariance.

Multi-edge subgraphs in multi-scales. For the construction of multi-edge subgraphs in different scales, different prefix thresholds r1, r2, and r3 are assigned separately. Therefore,  for dij≤r1, the multi-edge subgraph satisfies periodic invariance by using all terms in the set {dij|dij=||pi-pj+k1l1+k2l2+k3l3||2, k1, k2,k3∈Z,dij≤r1} to form edges between nodes i and j.  for r1<dij≤r2, the multi-edge subgraph satisfies periodic invariance by using all terms in the set {dij|dij=||pi-pj+k1l1+k2l2+k3l3||2, k1, k2,k3∈Z, r1<dij≤r2} to form edges between nodes i and j.  for r2<dij≤r3, the multi-edge subgraphs satisfy periodic invariance by using all terms in the {dij|dij=||pi-pj+k1l1+k2l2+k3l3||2, k1, k2,k3∈ Z, r2<dij≤r3} to form edges between nodes i and j. For each scale, the pairwise euclidean distances dij between all nodes i with position coordinates {pi=pi+k1l1+k2l2+k3l3, k1, k2,k3∈Z} and nodes j with position coordinates {pj=pj+k1l1+k2l2+k3l3, k1, k2,k3∈Z} are considered. It can be seen that for the same pair of pi and pj, dij remains unchanged when the periodic boundary moves. Therefore, this method satisfies period invariance. Furthermore, using pairwise euclidean distances, unit cell E(3) invariance is naturally satisfied.

S3. Performance of MHACGN-MS for gas adsorption prediction under different activation functions.

The performance of the MHACGN-MS model was evaluated across single-component (CO2) and multi-component (CO2 in CO2/N2 mixture) gas adsorption prediction tasks in Table S3, with particular focus on the impact of activation function combinations. As demonstrated in Table S3, the sigmoid + softplus configuration achieved superior performance due to its synergistic properties in handling complex graph-structured data. In crystal graphs characterized by significant noise (e.g., redundant interatomic interactions), sigmoid’s bounded normalization facilitates stable numerical computation by mapping interaction strengths to a probabilistic confidence interval [0, 1], thereby acting as an adaptive weighting mechanism for edge importance. Concurrently, softplus’s continuous differentiability ensures smooth gradient flow, which is critical for mitigating abrupt gradient variations during optimization and enhancing convergence stability in pooling operations. The ReLU + LeakyReLU combination secured the second-best performance, attributable to ReLU’s ability to induce beneficial sparsity and LeakyReLU’s negative slope mechanism, which prevents “neuron death” by maintaining nonzero gradients in the negative regime. The third-ranked tanh + LeakyReLU configuration likely underperformed due to tanh’s inherent susceptibility to gradient saturation, which limits effective gradient propagation compared to nonsaturating alternatives. Notably, the tanh + ReLU combination exhibited the poorest performance, as ReLU’s hard zero interval in the negative domain exacerbates the risk of irreversible neuron inactivation (zero gradients), while tanh’s bidirectional saturation regions further amplify training instability. This compounding effect severely restricts the network’s capacity for effective parameter adaptation, particularly in scenarios requiring fine-grained discrimination of weak interatomic interactions.

Table S3

Performance of MHACGN-MS based on different activation functions

| Selection of activation functions | CO2 |  | CO2:N2 (CO2) |  |
| --- | --- | --- | --- | --- |
|  | RMSE | R2 | RMSE | R2 |
| Sigmoid + softplus | 1.1891 | 0.9178 | 1.2584 | 0.8522 |
| Tanh + ReLU | 1.9822 | 0.7514 | 1.8103 | 0.7128 |
| Tanh + LeakyReLU | 1.6093 | 0.8674 | 1.7137 | 0.8017 |
| ReLU + LeakyReLU | 1.4513 | 0.8781 | 1.6272 | 0.8185 |

S4. Performance of MHACGN-MS for gas adsorption prediction under different pooling parameter r settings.

The impact of the pooling parameter kp on prediction performance deserves further discussion. When kp falls within the range of (0, 1], an excessively large kp retains redundant interatomic interactions, while an overly small kp leads to the loss of crucial interatomic information, thereby affecting prediction accuracy. Therefore, we evaluate kp values of 0.3, 0.5, 0.6, 0.7, 0.8, 0.9, and 1.0 to determine the optimal setting.

As can be seen from Tables S4 and S5, MHACGN-MS performs better when kp is set from 0.5 to 0.9 (compared to kp = 0.3 or 1.0). Meanwhile, we know that kp determines the size of the pooled graph, which in turn affects the complexity of subsequent computations and resource consumption. A larger kp results in a relatively larger size of the pooled graph, requiring more memory to store the graph’s structural information and edge features. This may lead to subsequent graph convolution layers or fully connected layers processing more edges, thereby increasing computation time. When kp = 0.6, MHACGN-MS demonstrates the optimal predictive performance. In this scenario, the attention pooling layer not only eliminates the interference from redundant interatomic interactions but also retains and emphasizes the information of key interatomic influences, while minimizing memory usage and enhancing computational speed. Therefore, when performance is similar, we choose 0.6 as the value for kp.

Table S4

The performance of MHACGN-MS for single-component gas adsorption prediction under different pooling parameter kp settings.

| Task | kp | RMSE (train) | RMSE (val) | RMSE (test) | R2 (train) | R2 (val) | R2 (test) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CH4 | 0.3 | 0.7089 | 0.8166 | 0.8322 | 0.8486 | 0.8259 | 0.8217 |
|  | 0.5 | 0.6703 | 0.7718 | 0.7925 | 0.8785 | 0.8546 | 0.8283 |
|  | 0.6 | 0.6573 | 0.7543 | 0.7876 | 0.8911 | 0.8633 | 0.8353 |
|  | 0.7 | 0.6686 | 0.7551 | 0.7901 | 0.8895 | 0.8629 | 0.8317 |
|  | 0.8 | 0.6607 | 0.7548 | 0.7913 | 0.8903 | 0.8631 | 0.8328 |
|  | 0.9 | 0.6583 | 0.7601 | 0.7804 | 0.8902 | 0.8620 | 0.8379 |
|  | 1.0 | 0.6740 | 0.7871 | 0.8158 | 0.8635 | 0.8331 | 0.8240 |
| CO2 | 0.3 | 1.2689 | 1.1848 | 1.2877 | 0.8841 | 0.8918 | 0.8794 |
|  | 0.5 | 1.2104 | 0.9782 | 1.2294 | 0.8873 | 0.9182 | 0.8973 |
|  | 0.6 | 1.1473 | 0.8935 | 1.1881 | 0.9092 | 0.9471 | 0.9203 |
|  | 0.7 | 1.1682 | 0.9419 | 1.2087 | 0.9047 | 0.9276 | 0.9132 |
|  | 0.8 | 1.1836 | 0.9327 | 1.2203 | 0.9002 | 0.9252 | 0.9039 |
|  | 0.9 | 1.1528 | 0.9393 | 1.2165 | 0.9006 | 0.9288 | 0.9107 |
|  | 1.0 | 1.2006 | 1.0273 | 1.2602 | 0.8895 | 0.9079 | 0.8904 |
| N2 | 0.3 | 0.4132 | 0.4861 | 0.4873 | 0.8485 | 0.8136 | 0.8122 |
|  | 0.5 | 0.3804 | 0.4329 | 0.4484 | 0.8632 | 0.8481 | 0.8319 |
|  | 0.6 | 0.3693 | 0.4194 | 0.4093 | 0.8819 | 0.8624 | 0.8438 |
|  | 0.7 | 0.3649 | 0.4228 | 0.4362 | 0.8934 | 0.8568 | 0.8322 |
|  | 0.8 | 0.3707 | 0.4283 | 0.4401 | 0.8805 | 0.8611 | 0.8301 |
|  | 0.9 | 0.3479 | 0.4433 | 0.4542 | 0.8977 | 0.8307 | 0.8247 |
|  | 1.0 | 0.3932 | 0.4476 | 0.4589 | 0.8521 | 0.8292 | 0.8209 |

Table S5

The performance of MHACGN-MS for multi-component gas adsorption prediction under different pooling parameter kp settings.

| Task | kp | Gas | RMSE (train) | RMSE (val) | RMSE (test) | R2 (train) | R2 (val) | R2 (test) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CH4:CO2 | 0.3 | CH4 | 1.7396 | 1.9052 | 2.1631 | 0.7561 | 0.7009 | 0.6909 |
|  |  | CO2 | 0.5707 | 0.5951 | 0.6559 | 0.8541 | 0.8329 | 0.8268 |
|  | 0.5 | CH4 | 1.7073 | 1.8784 | 2.1796 | 0.7728 | 0.7161 | 0.6942 |
|  |  | CO2 | 0.5475 | 0.5586 | 0.6233 | 0.8832 | 0.8583 | 0.8481 |
|  | 0.6 | CH4 | 1.6849 | 1.8624 | 2.1179 | 0.7881 | 0.7249 | 0.7120 |
|  |  | CO2 | 0.5219 | 0.5410 | 0.6057 | 0.8980 | 0.8669 | 0.8676 |
|  | 0.7 | CH4 | 1.6927 | 1.8463 | 2.2164 | 0.7735 | 0.7266 | 0.7061 |
|  |  | CO2 | 0.5195 | 0.5523 | 0.6215 | 0.8986 | 0.8711 | 0.8598 |
|  | 0.8 | CH4 | 1.8104 | 1.8788 | 2.1878 | 0.7699 | 0.7188 | 0.6972 |
|  |  | CO2 | 0.5202 | 0.5596 | 0.6276 | 0.8990 | 0.8619 | 0.8591 |
|  | 0.9 | CH4 | 1.7076 | 1.8557 | 2.1474 | 0.7668 | 0.7253 | 0.7082 |
|  |  | CO2 | 0.5078 | 0.5477 | 0.5990 | 0.8994 | 0.8605 | 0.8584 |
|  | 1.0 | CH4 | 1.7058 | 1.8917 | 2.1478 | 0.7593 | 0.7110 | 0.6977 |
|  |  | CO2 | 0.5561 | 0.5623 | 0.6456 | 0.8724 | 0.8699 | 0.8413 |
| CO2:N2 | 0.3 | CO2 | 1.3767 | 1.3558 | 1.3698 | 0.8355 | 0.8390 | 0.8362 |
|  |  | N2 | 0.6566 | 0.6828 | 0.7231 | 0.7839 | 0.7613 | 0.7308 |
|  | 0.5 | CO2 | 1.3483 | 1.2049 | 1.2884 | 0.8518 | 0.8821 | 0.8458 |
|  |  | N2 | 0.6227 | 0.6452 | 0.6841 | 0.8214 | 0.7738 | 0.7769 |
|  | 0.6 | CO2 | 1.3318 | 1.0988 | 1.2152 | 0.8585 | 0.8966 | 0.8778 |
|  |  | N2 | 0.6113 | 0.6292 | 0.6645 | 0.8362 | 0.7996 | 0.8206 |
|  | 0.7 | CO2 | 1.3362 | 1.1832 | 1.2168 | 0.8581 | 0.8872 | 0.8709 |
|  |  | N2 | 0.6183 | 0.6375 | 0.6803 | 0.8384 | 0.7835 | 0.7930 |
|  | 0.8 | CO2 | 1.3335 | 1.2193 | 1.2375 | 0.8588 | 0.8751 | 0.8633 |
|  |  | N2 | 0.6234 | 0.6426 | 0.7047 | 0.8337 | 0.7746 | 0.7756 |
|  | 0.9 | CO2 | 1.3119 | 1.2283 | 1.2313 | 0.8608 | 0.8607 | 0.8595 |
|  |  | N2 | 0.6130 | 0.6472 | 0.6836 | 0.8392 | 0.7738 | 0.7539 |
|  | 1.0 | CO2 | 1.3537 | 1.2413 | 1.2634 | 0.8471 | 0.8604 | 0.8383 |
|  |  | N2 | 0.6487 | 0.6694 | 0.6875 | 0.7771 | 0.7612 | 0.7344 |
| CH4:N2 | 0.3 | CH4 | 0.9388 | 0.9914 | 1.1480 | 0.7319 | 0.7352 | 0.6675 |
|  |  | N2 | 0.3614 | 0.4046 | 0.4076 | 0.8086 | 0.7558 | 0.7521 |
|  | 0.5 | CH4 | 0.9028 | 0.9519 | 1.0836 | 0.7530 | 0.7318 | 0.6837 |
|  |  | N2 | 0.3293 | 0.3610 | 0.3792 | 0.8395 | 0.7936 | 0.7826 |
|  | 0.6 | CH4 | 0.8882 | 0.9342 | 1.0037 | 0.7726 | 0.7424 | 0.7073 |
|  |  | N2 | 0.3128 | 0.3520 | 0.3638 | 0.8508 | 0.8127 | 0.8012 |
|  | 0.7 | CH4 | 0.8924 | 0.9514 | 0.9683 | 0.7638 | 0.7356 | 0.6995 |
|  |  | N2 | 0.3146 | 0.3589 | 0.3716 | 0.8501 | 0.8105 | 0.7936 |
|  | 0.8 | CH4 | 0.8836 | 0.9522 | 1.0091 | 0.7735 | 0.7335 | 0.7010 |
|  |  | N2 | 0.3255 | 0.3501 | 0.3494 | 0.8491 | 0.8128 | 0.8083 |
|  | 0.9 | CH4 | 0.8743 | 0.9453 | 1.0149 | 0.7734 | 0.7348 | 0.6979 |
|  |  | N2 | 0.3288 | 0.3424 | 0.3501 | 0.8487 | 0.8242 | 0.8067 |
|  | 1.0 | CH4 | 0.9192 | 0.9529 | 0.9763 | 0.7406 | 0.7201 | 0.7009 |
|  |  | N2 | 0.3335 | 0.3756 | 0.3949 | 0.8344 | 0.7998 | 0.7621 |

Using CO2 adsorption prediction as a case study, Table S6 analyzes how scale-specific kp values influence the learning of structural features. Notably, discussions of kp at a specific scale (e.g., 0–2 Å) assume default kp = 1.0 for other scales. For clarity, we denote kp values for 0–2, 2–3, and 3–5 Å as kp,1, kp,2, and kp,3, respectively.

As shown in Table S6:

(1) Adjusting kp,1 (0–2 Å): With kp,2 = kp,3 = 1.0, optimal performance occurs at kp,1 = 0.6. It suggests the 0–2 Å range contains redundant interatomic interactions requiring pruning (e.g., to isolate open metal sites/bonds).

(2) Adjusting kp,2 (2–3 Å): With kp,1 = kp,3 = 1.0, RMSE and R² show minimal variation, indicating limited interatomic interactions within this scale.

(3) Adjusting kp,3 (3–5 Å): With kp,1 =  kp,2 = 1.0, performance peaks at kp,3 = 0.8 before marginally declining at kp,3 = 1.0. This reflects the need for broader interatomic context to capture pore channel geometries, as excessively low kp,3 values (e.g., 0.3) impair structural feature learning.

Table S6

The influence of parameter kp settings at different scales on the performance of MHACGN-MS in predicting single component carbon dioxide adsorption.

| Scale | kp | RMSE (train) | RMSE (val) | RMSE (test) | R2 (train) | R2 (val) | R2 (test) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0–2 Å (kp,1) | 0.3 | 1.2592 | 1.1951 | 1.2902 | 0.8836 | 0.8877 | 0.8748 |
|  | 0.5 | 1.1394 | 0.9275 | 1.1694 | 0.9057 | 0.9218 | 0.9036 |
|  | 0.6 | 1.0031 | 0.8175 | 0.9373 | 0.9219 | 0.9396 | 0.9208 |
|  | 0.7 | 1.0957 | 0.8852 | 1.1016 | 0.9011 | 0.9288 | 0.9013 |
|  | 0.8 | 1.1748 | 0.9495 | 1.2174 | 0.8974 | 0.9118 | 0.9085 |
|  | 0.9 | 1.1563 | 0.9584 | 1.2246 | 0.8892 | 0.9028 | 0.8914 |
|  | 1.0 | 1.2006 | 1.0273 | 1.2602 | 0.8895 | 0.9079 | 0.8904 |
| 2–3 Å (kp,2) | 0.3 | 1.2183 | 0.9939 | 1.2634 | 0.8893 | 0.9081 | 0.8882 |
|  | 0.5 | 1.2017 | 0.9691 | 1.2447 | 0.8916 | 0.9148 | 0.8940 |
|  | 0.6 | 1.1936 | 0.9568 | 1.2364 | 0.8947 | 0.9194 | 0.9083 |
|  | 0.7 | 1.1985 | 0.9682 | 1.2482 | 0.8992 | 0.9127 | 0.8984 |
|  | 0.8 | 1.1963 | 0.9830 | 1.2535 | 0.8902 | 0.9095 | 0.9018 |
|  | 0.9 | 1.2158 | 1.0195 | 1.2619 | 0.8873 | 0.9046 | 0.8907 |
|  | 1.0 | 1.2006 | 1.0273 | 1.2602 | 0.8895 | 0.9079 | 0.8904 |
| 3–5 Å (kp,3) | 0.3 | 1.2825 | 1.1638 | 1.3152 | 0.8737 | 0.8884 | 0.8599 |
|  | 0.5 | 1.2151 | 1.0172 | 1.2637 | 0.8876 | 0.9038 | 0.8873 |
|  | 0.6 | 1.1927 | 0.9726 | 1.2422 | 0.8925 | 0.9122 | 0.9013 |
|  | 0.7 | 1.1828 | 0.9693 | 1.2565 | 0.9013 | 0.9089 | 0.8980 |
|  | 0.8 | 1.2006 | 1.0273 | 1.2602 | 0.8895 | 0.9079 | 0.8904 |
|  | 0.9 | 1.2173 | 1.0389 | 1.2684 | 0.8864 | 0.8984 | 0.8852 |
|  | 1.0 | 1.2495 | 1.0873 | 1.2815 | 0.8813 | 0.8922 | 0.8726 |

Conclusion:

(1) 0–2 Å (kp,1): Redundant interactions necessitate moderate pruning (kp,1 = 0.6) to enhance signal-to-noise ratio.

(2) 2–3 Å (kp,2): Limited interatomic interactions render kp,2 adjustments inconsequential for pore structure prediction.

(3) 3–5 Å (kp,3): Broader interatomic connectivity (kp,3 = 0.6–0.8) is critical for capturing extended pore geometries.

S5. Performance of different graph neural networks on the training and validation sets of single-component gas

Table S7

The performance of different graph neural networks on the training sets of single-component gas.

| Algorithm | CH4 |  | CO2 |  | N2 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | RMSE | R2 | RMSE | R2 | RMSE | R2 |
| MHACGN-MS | 0.6573 | 0.8911 | 1.1473 | 0.9092 | 0.3693 | 0.8819 |
| GCN | 0.9670 | 0.7633 | 1.5953 | 0.8269 | 0.4503 | 0.8203 |
| GAT | 1.4616 | 0.4587 | 3.1724 | 0.3306 | 0.5768 | 0.7064 |
| GIN | 0.8877 | 0.8001 | 1.2031 | 0.9003 | 0.4020 | 0.8593 |
| CGCNN | 0.7348 | 0.8629 | 1.1023 | 0.9189 | 0.3830 | 0.8725 |
| MEGNet | 0.7514 | 0.8564 | 1.5538 | 0.8374 | 0.4679 | 0.8067 |
| MPNN | 0.8371 | 0.8237 | 1.1496 | 0.9124 | 0.6267 | 0.6604 |
| MHACGN | 0.7644 | 0.8521 | 1.2488 | 0.8933 | 0.4252 | 0.8386 |

Table S8

The performance of different graph neural networks on the validation sets of single-component gas.

| Algorithm | CH4 |  | CO2 |  | N2 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | RMSE | R2 | RMSE | R2 | RMSE | R2 |
| MHACGN-MS | 0.7543 | 0.8633 | 0.8935 | 0.9471 | 0.4194 | 0.8624 |
| GCN | 1.0933 | 0.6981 | 1.7526 | 0.8031 | 0.5180 | 0.7916 |
| GAT | 1.4219 | 0.5051 | 3.2674 | 0.3057 | 0.5810 | 0.7323 |
| GIN | 0.7778 | 0.8383 | 1.3854 | 0.9011 | 0.4100 | 0.8463 |
| CGCNN | 0.8211 | 0.8147 | 1.0786 | 0.9401 | 0.3922 | 0.8556 |
| MEGNet | 0.7652 | 0.8507 | 1.7063 | 0.8050 | 0.4839 | 0.8253 |
| MPNN | 0.9877 | 0.7620 | 1.2085 | 0.9059 | 0.6973 | 0.5685 |
| MHACGN | 0.7813 | 0.8400 | 1.5245 | 0.8520 | 0.5211 | 0.7761 |

S6. Performance of different graph neural networks on the training and validation sets of multi-component gas

Table S9

The performance of graph neural networks on the training sets of multi-component gas.

| Algorithm | CH4:CO2 (CH4) |  | CO2:N2 (CO2) |  | CH4:N2 (CH4) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | RMSE | R2 | RMSE | R2 | RMSE | R2 |
| MHACGN-MS | 1.6849 | 0.7881 | 1.3319 | 0.8584 | 0.8882 | 0.7725 |
| GCN | 2.0075 | 0.7056 | 1.5855 | 0.7968 | 1.0237 | 0.7003 |
| GAT | 2.3015 | 0.6194 | 3.4219 | 0.0504 | 1.4566 | 0.3866 |
| GIN | 1.8189 | 0.7553 | 1.2955 | 0.8626 | 0.9037 | 0.7431 |
| CGCNN | 1.7548 | 0.7733 | 1.2782 | 0.8682 | 0.8951 | 0.7676 |
| MEGNet | 1.9259 | 0.7194 | 1.3870 | 0.8456 | 1.2721 | 0.5237 |
| MPNN | 2.5154 | 0.5326 | 1.4424 | 0.8334 | 1.4605 | 0.3942 |
| MHACGN | 1.7934 | 0.7645 | 1.2831 | 0.8671 | 0.9016 | 0.3361 |
| Algorithms | CH4:CO2 (CO2) |  | CO2:N2 (N2) |  | CH4:N2 (N2) |  |
|  | RMSE | R2 | RMSE | R2 | RMSE | R2 |
| MHACGN-MS | 0.5219 | 0.8980 | 0.6113 | 0.8362 | 0.3128 | 0.8508 |
| GCN | 0.7627 | 0.7810 | 0.7447 | 0.7628 | 0.3910 | 0.7666 |
| GAT | 1.4501 | 0.2164 | 0.8831 | 0.6594 | 0.4678 | 0.6684 |
| GIN | 0.5975 | 0.8646 | 0.5976 | 0.8423 | 0.3511 | 0.8113 |
| CGCNN | 0.6431 | 0.8464 | 0.6570 | 0.8114 | 0.3274 | 0.8345 |
| MEGNet | 0.6317 | 0.8508 | 0.8029 | 0.7349 | 0.3899 | 0.7707 |
| MPNN | 0.6911 | 0.8173 | 0.9479 | 0.6102 | 0.3470 | 0.8171 |
| MHACGN | 0.5318 | 0.8776 | 0.6313 | 0.8270 | 0.3361 | 0.8264 |

Table S10

The performance of graph neural networks on the validation sets of multi-component gas.

| Algorithm | CH4:CO2 (CH4) |  | CO2:N2 (CO2) |  | CH4:N2 (CH4) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | RMSE | R2 | RMSE | R2 | RMSE | R2 |
| MHACGN-MS | 1.8624 | 0.7249 | 1.0988 | 0.8966 | 0.9342 | 0.7423 |
| GCN | 2.5030 | 0.6083 | 1.6075 | 0.7978 | 1.1023 | 0.6411 |
| GAT | 2.4611 | 0.5912 | 3.5401 | 0.0429 | 1.5034 | 0.3725 |
| GIN | 2.0914 | 0.7048 | 1.5092 | 0.7817 | 0.9964 | 0.6919 |
| CGCNN | 1.9799 | 0.7600 | 1.4680 | 0.8374 | 0.9666 | 0.7280 |
| MEGNet | 2.0713 | 0.6885 | 1.7975 | 0.7689 | 1.4112 | 0.4893 |
| MPNN | 2.6584 | 0.4728 | 1.3723 | 0.8496 | 1.5199 | 0.2705 |
| MHACGN | 1.9348 | 0.7105 | 1.5822 | 0.8309 | 0.9845 | 0.7305 |
| Algorithm | CH4:CO2 (CO2) |  | CO2:N2 (N2) |  | CH4:N2 (N2) |  |
|  | RMSE | R2 | RMSE | R2 | RMSE | R2 |
| MHACGN-MS | 0.5411 | 0.8669 | 0.6292 | 0.7996 | 0.3520 | 0.8127 |
| GCN | 0.7517 | 0.8525 | 0.7367 | 0.7457 | 0.3931 | 0.7403 |
| GAT | 1.3301 | 0.2973 | 0.9313 | 0.6075 | 0.4964 | 0.6387 |
| GIN | 0.6744 | 0.8531 | 0.6770 | 0.7984 | 0.3752 | 0.8172 |
| CGCNN | 0.5846 | 0.8541 | 0.7179 | 0.7687 | 0.3461 | 0.8460 |
| MEGNet | 0.6327 | 0.8463 | 0.8512 | 0.7608 | 0.4094 | 0.7288 |
| MPNN | 0.8849 | 0.7734 | 1.0003 | 0.5838 | 0.3677 | 0.7832 |
| MHACGN | 0.6042 | 0.8520 | 0.7134 | 0.7750 | 0.3643 | 0.7955 |

S7. The computational resources and efficiency of MHACGN-MS.

All our models were developed on the Ubuntu 22.04 LTS operating system, utilizing the Python 3.12.4 programming language and the PyTorch 2.2.0 deep learning framework. In terms of hardware, we employed Intel Xeon Platinum 8358P CPUs, with dual CPUs each having 32 cores and 64 threads. The CPUs operate at a maximum frequency of 3.4 GHz, a base frequency of 2.6 GHz, and have a total cache capacity of 181 MB. Furthermore, we used four NVIDIA A800 PCIe GPUs, each with 80 GB of HBM2e memory.

Table S11 lists the total parameters (parameters), the time required for one epoch of model training (time), the memory allocated on the GPU (allocated memory), and the cached memory on the GPU (cached memory) as indicators to illustrate the time complexity (execution time) and space complexity (occupied storage space) of different models. Except for the total parameters, the remaining indicators were obtained by running each model for 20 episodes and calculating the average of the printed parameters to eliminate error interference. Among all models, GCN, GAT, and GIN have fewer total parameters compared to MHACGN-MS. However, this is because these models do not consider the edge information of crystal graphs. Although their model structures are simpler, their accuracy in predicting crystal material properties is lower. Among the models that consider edge information in crystal graphs, MHACGN-MS occupies the least GPU memory and cache. In terms of computational efficiency, MHACGN-MS is the fastest among all models. We believe this demonstrates that dividing crystal graphs into multi-scale subgraphs for separate learning effectively improves data quality and accelerates model computation speed.

Table S12 provides the specific parameters of the MHACGN-MS model to assist researchers who may wish to replicate the study or apply this method to different datasets.

Table S11

Explanation of the temporal and spatial complexity of models.

| Model | Parameter | Time per epoch (s) | Allocated memory (byte) | Cached memory (byte) |
| --- | --- | --- | --- | --- |
| MHACGN-MS | 560 405 | 52.72 | 26 680 320 | 7 850 303 232 |
| GCN | 357 255 | 53.49 | 24 312 832 | 1 277 165 568 |
| GAT | 362 055 | 53.25 | 24 587 264 | 6 203 375 616 |
| GIN | 521 255 | 54.26 | 27 614 208 | 5 167 382 528 |
| CGCNN | 702 765 | 54.34 | 31 220 736 | 7 941 914 624 |
| MEGNet | 875 909 | 53.54 | 34 718 720 | 9 871 294 464 |
| MPNN | 633 297 | 53.90 | 29 429 760 | 25 142 755 328 |
| MHACGN | 491 645 | 53.16 | 27 549 184 | 21 292 384 256 |

Table S12

Hyperparameters that are employed in MHACG-MS model.

| Hyperparameter | Value | Range |
| --- | --- | --- |
| Number of convolutional layers | 9 | 6–12 |
| Length of atom feature vector | 92 | 92 |
| Length of edge feature vector | 3 | 3 |
| Number of GraphPooling layers | 3 | 3 |
| Learning rate | 0.002 | 0.001–0.005 |