Supplementary data for

Functional Capsules Encapsulating Molecular-Recognizable Nanogels for Facile Removal of Organic Micro-Pollutants from Water

Wen-Ying Liu a, Xiao-Jie Ju a,b,*, Xing-Qun Pu a, Quan-Wei Cai a, Yu-Qiong Liu a, Zhuang Liu a,b, Wei Wang a,b, Rui Xie a,b, Liang-Yin Chu a,*

a School of Chemical Engineering & State Key Laboratory of Hydraulics and Mountain River Engineering, Sichuan University, Chengdu 610065, China

b State Key Laboratory of Polymer Materials Engineering, Sichuan University, Chengdu 610065, China

Fig. S1. Schematic illustration of fabrication of the proposed functional capsules encapsulating PNCD nanogels. (a, b) Schematic illustration of the synthesis of molecular-recognizable (b) PNCD nanogels by chemically grafting CD moieties onto (a) PNA nanogels (a1→b1) via EDC condensation (a2→b2). (c,d) Schematic illustration of the fabrication of the functional capsules with co-extrusion technique by dripping (c) water-in-water (W/W) droplet templates into a Ca(NO3)2 solution to form (d) stable capsules through the cross-linking of Ca2+-triggered sol-gel transition of the capsule shells. The inner fluid is aqueous CMC solution containing PNCD nanogels, and the outer fluid is aqueous Na-Alg solution.

Fig. S2. The FT-IR spectra of CD, PNA nanogels, and PNCD nanogels.

Fig. S3. SEM image of PNA nanogels in dried state.

Fig. S4. Adsorption characteristics of capsules containing 10 mg·mL–1 PNCD nanogels in each capsule toward 0.5 mmol·L–1 BPA in water at 25 °C. (a) Qt, (b) R, and (c) qt changes in the BPA adsorbed by different numbers of capsules. (d) Pseudo-second-order plots of BPA adsorbed by different numbers of capsules.

Fig. S5. Adsorption characteristics of capsules containing 15 mg·mL–1 PNCD nanogels in each capsule toward 0.5 mmol·L–1 BPA in water at 25 °C. (a) Qt, (b) R, and (c) qt changes in the BPA adsorbed by different numbers of capsules. (d) Pseudo-second-order plots of BPA adsorption by different numbers of capsules.

Fig. S6. Adsorption characteristics of capsules containing 20 mg·mL–1 PNCD nanogels in each capsule toward 0.5 mmol·L–1 BPA in water at 25 °C. (a) Qt, (b) R, and (c) qt changes in the BPA adsorbed by different numbers of capsules. (d) Pseudo-second-order plots of BPA adsorption by different numbers of capsules.

Fig. S7. Adsorption characteristics of capsules containing 30 mg·mL–1 PNCD nanogels in each capsule toward 0.5 mmol·L–1 BPA in water at 25 °C. (a) Qt, (b) R, and (c) qt changes in the BPA adsorbed by different numbers of capsules. (d) Pseudo-second-order plots of BPA adsorption by different numbers of capsules.

Fig. S8. Redlich-Peterson isothermal adsorption model of BPA adsorption by the capsules encapsulating 15 mg·mL–1 PNCD nanogels in each capsule at 25 C.

Table S1

The pseudo-second-order plots results of BPA adsorption by capsules encapsulated with different concentrations of PNCD nanogels for 0.5 mmol·L–1 BPA-containing solutions.

| [PNCD] (mg·mL–1) | No. of capsule | Pseudo-second-order model | R2 | qe,exp (mg·g–1) | qe,cal (mg·g–1) | Kobs (g·mg–1·min–1) |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | 5 | y = 0.0115x + 0.0966 | 0.9997 | 85.2479 | 86.9565 | 0.0014 |
|  | 10 | y = 0.0141x + 0.0746 | 0.9995 | 70.0686 | 70.9220 | 0.0038 |
|  | 20 | y = 0.0170x + 0.1065 | 0.9996 | 57.9048 | 58.8235 | 0.0027 |
|  | 30 | y = 0.0183x + 0.1244 | 0.9999 | 53.8502 | 54.6448 | 0.0027 |
|  | 40 | y = 0.0222x + 0.0999 | 0.9999 | 44.5806 | 45.0450 | 0.0049 |
| 10 | 5 | y = 0.0138x + 0.3280 | 0.9991 | 68.5439 | 72.4638 | 0.0006 |
|  | 10 | y = 0.0159x + 0.2821 | 0.9995 | 60.1918 | 62.8931 | 0.0009 |
|  | 20 | y = 0.0218x + 0.2735 | 0.9996 | 44.5806 | 45.8716 | 0.0020 |
|  | 30 | y = 0.0304x + 0.2450 | 0.9999 | 32.2616 | 32.8947 | 0.0038 |
|  | 40 | y = 0.0382x + 0.1891 | 0.9999 | 25.9115 | 26.1780 | 0.0077 |
| 15 | 5 | y = 0.0152x + 0.6077 | 0.9976 | 59.9264 | 65.7895 | 0.0004 |
|  | 10 | y = 0.0195x + 0.7024 | 0.9974 | 47.2432 | 51.2821 | 0.0005 |
|  | 20 | y = 0.0298x + 0.4127 | 0.9998 | 32.2616 | 33.5570 | 0.0022 |
|  | 30 | y = 0.0423x + 0.4673 | 0.9998 | 23.0324 | 23.6407 | 0.0038 |
|  | 40 | y = 0.0572x + 0.2586 | 0.9999 | 17.7825 | 17.4825 | 0.0127 |
| 20 | 5 | y = 0.0179x + 1.2507 | 0.9955 | 47.9942 | 55.8659 | 0.0005 |
|  | 10 | y = 0.0243x + 1.2251 | 0.9994 | 37.3383 | 41.1523 | 0.0005 |
|  | 20 | y = 0.0409x + 0.9503 | 0.9996 | 23.2432 | 24.4499 | 0.0018 |
|  | 30 | y = 0.0592x + 0.7492 | 0.9998 | 16.3849 | 16.8919 | 0.0047 |
|  | 40 | y = 0.0745x + 0.4174 | 0.9999 | 13.2416 | 13.4228 | 0.0133 |
| 30 | 5 | y = 0.0226x + 1.7425 | 0.9967 | 38.6032 | 44.2478 | 0.0003 |
|  | 10 | y = 0.0348x + 1.4342 | 0.9975 | 26.6710 | 28.7356 | 0.0008 |
|  | 20 | y = 0.0590x + 1.3090 | 0.9991 | 16.2578 | 16.9491 | 0.0027 |
|  | 30 | y = 0.0866x + 0.9190 | 0.9997 | 11.2621 | 11.5473 | 0.0082 |
|  | 40 | y = 0.1082x + 0.7712 | 0.9999 | 9.0819 | 9.2421 | 0.0152 |