Supplementary Data for

# Remarkable Enhancement of the Activity and Hydrothermal Stability of a CeO2-Based NH3-SCR Catalyst by Sn Modification

Ying Zhu a,d,#, Jingjing Liu c,#, Guangzhi He c, Shaohua Xie e, Wenpo Shan a,b,*, Zhihua Lian a, Fudong Liu e, Hong He a,c,d,*

a Center for Excellence in Regional Atmospheric Environment & Key Laboratory of Urban Pollutant Conversion, Institute of Urban Environment, Chinese Academy of Sciences, Xiamen 361021, China

b Zhejiang Key Laboratory of Pollution Control for Port-Petrochemical Industry, Ningbo Urban Environment Observation and Research Station, Institute of Urban Environment, Chinese Academy of Sciences, Ningbo 315800, China

c State Key Joint Laboratory of Environment Simulation and Pollution Control, Research Center for Eco-Environmental Sciences, Chinese Academy of Sciences, Beijing 100085, China

d University of Chinese Academy of Sciences, Beijing 100049, China

e Department of Civil, Environmental and Construction Engineering, Catalysis Cluster for Renewable Energy and Chemical Transformations, NanoScience Technology Center, University of Central Florida, Orlando, FL 32816, USA

# These authors contributed equally to this work.

* Corresponding authors.

E-mail addresses: wpshan@iue.ac.cn (W. Shan), honghe@rcees.ac.cn (H. He).

Catalyst preparation and hydrothermal aging treatment

The Ce–Sn–Nb mixed oxide (denoted as Ce1SnaNb1Ox, where a = 0.5, 1.0, 1.5, 2.0, 2.5, and 3.0) was synthesized by a co-precipitation method using NH3·H2O as the precipitator. The required amounts of Ce(NO3)3∙6H2O, SnCl4∙5H2O, and C10H5NbO20 were firstly dissolved together in deionized water. Excessive NH3∙H2O was then added to the mixed slurry, dropwise, and the mixture was stirred continuously at room temperature overnight. After filtration and washing with plenty of deionized water, the resulting precipitate was dried at 100 °C for 8 h and subsequently calcined at 700 °C for 3 h in air condition. CeO2, SnO2, Nb2O5, Ce1Sn2Ox, Sn2Nb1Ox, and Ce1Nb1Ox samples were also prepared using the same method for comparison. The calcined powder catalysts were finally pressed, crushed, and sieved to 40–60 mesh for SCR activity evaluation.

Catalyst characterization

X-ray diffraction (XRD) patterns of the catalysts were collected on a computerized X’Pert PRO diffractometer with Cu Kα radiation operated at 40 kV and 40 mA. The data were recorded with 2θ ranging from 5° to 90° and scan step size of 0.02°.

In-situ high temperature XRD (HTXRD) measurements were carried out to investigate the phase evolution at high temperature using a Bruker D8 Advance diffractometer equipped with a Cu Kα X-ray tube (1.5418 Å) operated at 40 kV and 40 mA. The Ce1Nb1Ox and Ce1Sn2Nb1Ox powder samples were placed in a crucible, heating from 600 to 1000 °C with a temperature interval of 50 °C, and then cooled down to room temperature. After the catalysts reached the target temperature and maintained stability, the XRD data collection started recording. A counting time per step of 0.6 s and a step size of 0.02° were selected for the angular range 20°–90° 2θ in the temperature programmed process.

N2 adsorption–desorption analysis of catalysts was conducted at a liquid nitrogen temperature (−196 °C) using a physisorption analyzer (MicrotracBEL). Prior to the N2 physisorption test, all of the samples were degassed at 300 °C for 1 h under vacuum. Specific surface area and pore volume of catalysts were measured by the Brunauer–Emmett–Teller (BET) and Barrett–Joyner–Halenda (BJH) models, respectively.

The morphologies and elements distribution of catalysts were explored by a high-resolution transmission electron microscope (HRTEM) equipped with energy-dispersive X-ray spectroscopy (EDS), which was operated on a JEOL 3200F instrument at an accelerating voltage of 300 kV.

The temperature-programmed reduction of hydrogen (H2-TPR) and the temperature-programmed desorption of NH3 (NH3-TPD) experiments were performed with a Micromeritics Autochem Ⅱ 2920 automatic chemisorption analyzer. The signals were monitored by a thermal conductivity detector (TCD). Prior to H2-TPR and NH3-TPD analysis, all of the samples were firstly pre-treated under a flow of pure Ar (30 mL∙min−1) at 400 °C for 30 min, and then cooled down to the room temperature. For H2-TPR, the samples were heated from room temperature to 1000 °C under 10 vol% H2/Ar mixture gas flow (50 mL∙min−1) in a U-shaped quartz tube at a heating rate of 10 °C∙min−1. For NH3-TPD, the catalysts were exposed to 2500 ppm NH3/He mixture gas flow of 30 mL∙min−1 at room temperature for 1 h, followed by pure Ar (30 mL∙min−1) purge for 2 h. Finally, the temperature was raised to 550 °C at a constant rate of 10 °C∙min−1. All spectra were collected every second. Liquid nitrogen was added to remove the effects of water prior to collection.

X-ray photoelectron spectroscopy (XPS) measurements were collected on an AXIS Supra (Kratos Analytical Inc.) using monochromatized Al Kα radiation (λ = 1486.6 eV) as X-ray source. The binding energies of Ce 3d, Nb 3d, Sn 3d, and O 1s were calibrated by C 1s signal (binding energy (BE) = 284.8 eV) as standard.

X-ray absorption near edge structure (XANES) and extended X-ray absorption fine structure (EXAFS) of the Nb K-edge and XANES of the Ce L3-edge, Sn K-edge, and Nb K-edge were measured in a transmission mode at room temperature at beamline 7-BM QAS of the National Synchrotron Light Source II (NSLS-II), Brookhaven National Laboratory (BNL). Data were analyzed using Athena and Artemis from the Demeter software package. The filtered k3-weighted χ(k) was Fourier transformed into R space in the k range of 3.0–13.5 Å−1 for Nb K-edge.

The in-situ diffuse reflectance infrared Fourier transform spectra (DRIFTS) employing a Fourier-transform infrared spectrometer (FTIR, Nicolet IS50) equipped with a Smart Collector, an MCT/A detector using liquid nitrogen for cooling, and an in-situ DRIFTS cell including ZnSe window. An Omega programmable temperature controller was used for controlling the reaction temperature. Prior to each experiment, the catalysts were pre-treated under 20 vol% O2/N2 mixture gas flow at 450 °C for 30 min to remove the adsorbed impurities, and then cooled down to 200 °C. The background spectra were collected in pure N2 (300 mL∙min−1) and subtracted from the catalyst spectra. The catalysts spectra were collected ranging from 4000 to 600 cm−1 when the samples were exposed to the atmospheres of 500 ppm NH3 and balance N2, with a total flow rate of 300 mL∙min−1. For each sample, the NH3 adsorption time was controlled at least 1 h to ensure complete adsorption. Subsequently, the catalysts were purged to eliminate the effects of physical adsorption by nitrogen for another 1 h until the FTIR spectra were stabilized. All spectra were obtained at 4 cm−1 resolution with 100 accumulated scans.

Density functional theory (DFT) calculations

The projector augmented wave (PAW) method was used to describe the core–valence electron interaction [1]. DFT + U approach was applied to the Nb atom in NbOx and Ce atom in CeOx with the values of Ueff = 4.0 and 4.5 eV, respectively, to describe the on-site Coulomb interactions [2,3]. The plane wave energy cutoff was set to 400 eV for all atoms. A (4 × 2) supercell of the SnO2(110) surface with three stoichiometric SnO2 layers was used as the substrate. For the calculation of formation energy of NbOx, CeOx, and NbCeOx species on SnO2 surfaces, the bottom one stoichiometric SnO2 layer was kept frozen at their bulk position, whereas all other atoms were fully relaxed. For the calculation of the surface energy of SnO2 and NbOx/CeOx/NbCeOx-loaded SnO2, all atoms were fully relaxed. The Brillouin zone was sampled at the Γ point. A vacuum spacing of 20 Å was used to avoid the periodic image interaction normal to the surface. The convergence tolerances of energy and force were 10−5 eV and 0.02 eV∙Å−1, respectively. The Gaussian smearing method with a smearing width of 0.05 eV was applied to improve the convergence for Brillouin zone integration.

Results

The NH3-SCR activities over Ce1SnaNb1Ox catalysts at a gas hourly space velocity (GHSV) of 100 000 h−1 were shown in Fig. S1(a). The Ce1Nb1Ox catalyst already exhibited high NH3-SCR activity over a wide temperature range. After the addition of Sn, the low temperature activity of the catalyst was gradually enhanced with the increment of Sn/Ce molar ratio. However, after further increasing the Sn/Ce molar ratio to 2.5 and 3.0, the high temperature activity above 450 °C slightly decreased, accompanying with a decrease of N2 selectivity (Fig. S1(b)). All conditions considered, the Ce1Sn2Nb1Ox catalyst with the Ce:Sn:Nb molar ratio of 1:2:1 was selected and tested for hydrothermal stability in this study.

Fig. S1. The (a) NOx conversion and (b) N2 selectivity of the catalysts with various Sn/Ce molar ratios. Reaction conditions: [NO] = [NH3] = 500 ppm, [O2] = 5 vol%, [H2O] = 5 vol%, balance N2, and gas hourly space velocity (GHSV) = 100 000 h−1.

Fig. S2. The N2 selectivity of hydrothermally aged catalysts. Reaction conditions: [NO] = [NH3] = 500 ppm, [O2] = 5 vol%, [H2O] = 5 vol%, balance N2, and GHSV = 100 000 h−1.

Fig. S3. (a) The Rietveld refinement profiles of CeO2, SnO2, Ce1Sn2Ox, and Ce1Sn2Nb1Ox. (b) XRD patterns of SnO2, Ce1Sn2Ox, and Ce1Sn2Nb1Ox catalysts in the range of 23°–31°.

Fig. S4. In-situ HTXRD patterns of (a) Ce1Nb1Ox and (b) Ce1Sn2Nb1Ox catalysts.

Fig. S5. The HRTEM images of (a) Ce1Nb1Ox, (b) Ce1Nb1Ox-800, (c) Ce1Nb1Ox-900, (d) Ce1Nb1Ox-1000, (e) Ce1Sn2Nb1Ox, (f) Ce1Sn2Nb1Ox-800, (g) Ce1Sn2Nb1Ox-900, and (h) Ce1Sn2Nb1Ox-1000  catalysts.

The Ce 3d spectra were decomposed into eight overlapping peaks, which were labeled as μ, μ′, μ″, μ‴, ν, ν′, ν″, and ν‴, respectively. Among them, the peaks of μ, μ″, μ‴, ν, ν″, and ν‴ are associated with 3d104f0 initial electronic state of Ce4+, and the peaks of μ′ and ν′ represent the 3d104f1 initial electronic state of Ce3+ [4,5]. The results indicated that Ce species were dominated by Ce4+, along with some Ce3+ [6]. To compare the chemical state of Ce over different catalysts intuitively, the Ce3+/Ce ratios were calculated by the following equation and marked in the Figs. S6(a) and (b).

Ce3+/Ce=Ce3+/Ce3++Ce4+=Sμ'+S(ν')Sμ+Sν×100% 				(S1)

where S(μ′), S(ν′), S(μ), and S(ν) denote the peak areas of μ′, ν′, μ, and ν.

After the addition of Sn, the Ce 3d peaks of Ce1Sn2Nb1Ox catalysts appeared at lower binding energies compared with Ce1Nb1Ox catalysts, while the peaks of Nb 3d shifted to higher binding energies (Fig. S6(c)). It indicates that the addition of Sn could induce the stronger interaction between Ce and Nb species, which might be an important reason for the better low-temperature activity of Ce1Sn2Nb1Ox than Ce1Nb1Ox catalyst.

Fig. S6. XPS results of (a, b) Ce 3d, (c) Nb 3d, and (d) Sn 3d for the catalysts.

The O 1s XPS spectra were well split into two components, which were illustrated in Fig. S7. The peaks of higher binding energy (531.8 eV) were assigned to the surface chemisorbed oxygen (O22− or O−, denoted as Oα), while the peaks of lower binding energy (529.9–530.4 eV) were ascribed to the lattice oxygen (O2−, denoted as Oβ) [7,8]. The Oα/O ratios were calculated by the following formula and marked in the Fig. S7.

Oα/O=Oα/Oα+Oβ=S(Oα)SOα+S(Oβ)×100%						(S2)

where S(Oα) and S(Oβ) denote the peak areas of Oα and Oβ.

It was found that the binding energy of Oβ moved higher with Sn introduction. Because the electronegativity of Sn (1.96) was larger than that of Ce (1.10), it meant that the electron capture ability of Sn was stronger [9,10]. Meanwhile, the Oα/O ratio increased after the doping of Sn. As the Oα is active in oxidation reactions, the higher Oα/O ratio could facilitate the oxidation of NO [11]. These may account for the better low-temperature performance of Ce1Sn2Nb1Ox than Ce1Nb1Ox catalyst.

Fig. S7. XPS spectra for O 1s of fresh and hydrothermally aged (a) Ce1SNb1Ox and (b)Ce1Sn2Nb1Ox catalysts.

The normalized Ce L3-edge XANES spectra of catalysts were shown in Fig. S8(a), along with CeO2, Ce(NO3)3, Nb2O5, and NbO2 as references. For the spectrum of Ce(NO3)3, a strong absorption peak (C) at 5726.4 eV is due to the transition from Ce 2p to Ce 4f15d [12,13]. As for CeO2, a weak pre-edge absorption peak (D) at 5720.6 eV is ascribed to the O 2p–Ce 5d hybridizations [14–16]. Two strong absorption peaks (A, B) centered at 5737.3 and 5730.7 eV are assigned to the transitions from Ce 2p3/2 to Ce 4f15dL and Ce 2p3/2 to Ce 4f05d, respectively, where 4f15dL represents that Ce 4f borrowing an electron from its oxygen neighbors and leaving an O 2p hole (L) [12,17,18]. In Fig. S8(a), the XANES spectrum of Ce1Nb1Ox exhibited a peak shape similar to CeO2. In the case of Ce1Nb1Ox-900, Ce1Sn2Nb1Ox, and Ce1Sn2Nb1Ox-900, the spectra showed a strong peak at 5726.4 eV, characteristic of Ce3+, and two peaks characteristic of Ce4+ appeared at 5737.3 and 5730.7 eV. It could be observed that Ce3+ and Ce4+ co-existed in the above catalysts.

Fig. S8. XANES spectra for (a) Ce L3-edge and (b) Nb K-edge of the catalysts.

To examine the valence states of constituent elements, the Ce L3-edge of catalysts were fitted to four peaks (peaks A–D) by arctangent and Gaussian function (Fig. S9) [14].

Ce3+/Ce=Ce3+/Ce3++Ce4+=SCSA+SB+SC×100%				(3)

where S(A), S(B), and S(C) denote the peak areas of A, B, and C, respectively [19].

In Fig. S9, the peak area with the orange shade is related to an amount of Ce3+, and an area sum of two peaks with blue and green shades is assigned to an amount Ce4+. The percentages of Ce3+/Ce in Ce1Nb1Ox, Ce1Nb1Ox-900, Ce1Sn2Nb1Ox, and Ce1Sn2Nb1Ox-900 were calculated to be 15.6%, 38.8%, 39.3%, and 40.1%, respectively, which exhibited the same trend as the XPS results. Both of the introduction of Sn and hydrothermal aging treatment could increase the ratio of Ce3+/Ce due to the formation of Ce3+-associated new crystal phase.

Fig. S9. XANES spectra fitting for Ce L3-edge of the (a) Ce1Nb1Ox, (b) Ce1Sn2Nb1Ox, (c) Ce1Nb1Ox-900, and (d) Ce1Sn2Nb1Ox-900 catalysts.

The normalized Nb K-edge XANES spectra of catalysts were shown in Fig. S8(b). NbO2 and Nb2O5 were used as references. The spectra were deconvoluted to one weak absorption peak at 18 981.7 eV in the pre-edge region and two post-edge peaks centered at 18 999.1 and 19 011.3 eV. The pre-edge peak is due to the s–d transitions and the intensity depends on the coordination [20,21]. The niobium species in the four samples and in the Nb2O5 reference showed very similar XANES features, which revealed that all four samples were dominated by Nb2O5. According to the previous study, the pre-edge peak intensity in XANES spectra was positively correlated with the structural distortion of specific element [22]. In our case, as shown in Fig. S8(b) inset, the pre-edge peak of Ce1Nb1Ox catalyst exhibited an obvious decrease in intensity with the increase of hydrothermal aging temperature, whereas there was almost no change in pre-edge peak intensity of Ce1Sn2Nb1Ox catalyst. The XANES results indicated that the coordination structures of Nb species in Ce1Nb1Ox catalyst were transformed by severely hydrothermal aging, while that in Ce1Sn2Nb1Ox catalyst remained stable. Therefore, the addition of Sn stabilized the coordination structures of Nb species in Ce1Sn2Nb1Ox catalyst.

The in-situ DRIFTS experiments of fresh and hydrothermally aged catalysts were carried out, and the results are shown in Fig. S10. The negative bands at 1961 and 1966 cm−1 attributed to the stretching mode of Nb=O in the overtone region [23] could be observed for Ce1Sn2Nb1Ox and Ce1Sn2Nb1Ox-800 catalysts, indicating that Nb=O can serve as acid site for NH3 adsorption [24–26]. Meanwhile, the intensity of the Nb=O consumption peak of Ce1Sn2Nb1Ox-800 was significantly weaker than that in Ce1Sn2Nb1Ox. Although the surface Nb concentration of Ce1Sn2Nb1Ox-800 was higher than that of Ce1Sn2Nb1Ox, its Nb species as acid sites decreased due to the decrease of surface area during hydrothermal aging.

Fig. S10. Magnified in-situ DRIFTS results of NH3 adsorption at 200 °C on catalysts from 2000 to 1900 cm−1.

Table S1

The lattice parameters extracted from Rietveld refinement results.

| Sample | c-CeO2 (Fm-3m) |  | t-SnO2 (P42/mnm) |  |  | m-CeNbO4.25 (I2/a) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | a (Å) | V (Å3) | a (Å) | c (Å) | V (Å3) | a (Å) a) | b (Å) b) | c (Å) c) | V (Å3) d) |
| CeO2 | 5.412(0) | 158.50 | — | — | — | — | — | — | — |
| SnO2 | — | — | 4.738(0) | 3.187(0) | 71.55 | — | — | — | — |
| Ce1Sn2Ox | 5.404(1) | 157.81 | 4.749(1) | 3.213(1) | 72.47 | — | — | — | — |
| Ce1Sn2Nb1Ox | 5.403(1) | 157.75 | 4.746(1) | 3.174(1) | 71.49 | — | — | — | — |
| Ce1Sn2Nb1Ox-800 | 5.409(0) | 158.28 | 4.740(0) | 3.171(1) | 71.25 | — | — | — | — |
| Ce1Sn2Nb1Ox-900 | 5.411(0) | 158.42 | 4.731(0) | 3.186(1) | 71.32 | 5.475(4) | 11.187(5) | 5.148(3) | 314.77 |
| Ce1Sn2Nb1Ox-1000 | 5.419(1) | 159.09 | 4.740(1) | 3.178(1) | 71.42 | 5.351(1) | 11.384(2) | 5.139(1) | 312.61 |

a, b, and c are three lattice parameters in three-dimensional space; V is cell volume.

Table S2

The surface elemental compositions of fresh and hydrothermally aged catalysts.

| Sample | Element compositions (%) |  |  |  | Elemental composition ratio |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ce | Sn | Nb | O | Nb/Ce | Ce/Sn | Nb/Sn |
| Ce1Nb1Ox | 13.8 | — | 17.4 | 68.7 | 1.26 | — | — |
| Ce1Nb1Ox-800 | 13.2 | — | 17.8 | 69.0 | 1.35 | — | — |
| Ce1Nb1Ox-900 | 15.2 | — | 16.5 | 68.3 | 1.08 | — | — |
| Ce1Nb1Ox-1000 | 14.5 | — | 18.5 | 67.0 | 1.28 | — | — |
| Ce1Sn2Nb1Ox | 7.8 | 16.2 | 9.8 | 66.1 | 1.26 | 0.48 | 0.61 |
| Ce1Sn2Nb1Ox-800 | 6.2 | 16.2 | 11.2 | 66.4 | 1.81 | 0.38 | 0.69 |
| Ce1Sn2Nb1Ox-900 | 5.8 | 17.2 | 10.9 | 66.1 | 1.87 | 0.34 | 0.63 |
| Ce1Sn2Nb1Ox-1000 | 5.5 | 19.4 | 9.7 | 65.5 | 1.77 | 0.28 | 0.50 |

References

[1] Kresse G, Joubert D. From ultrasoft pseudopotentials to the projector augmented-wave method. Phys Rev B 1999;59(3):1758–75.

[2] Koçer CP, Griffith KJ, Grey CP, Morris AJ. First-principles study of localized and delocalized electronic states in crystallographic shear phases of niobium oxide. Phys Rev B 2019;99(7):075151.

[3] Park JB, Graciani J, Evans J, Stacchiola D, Ma S, Liu P, et al. High catalytic activity of Au/CeOx/TiO2(110) controlled by the nature of the mixed-metal oxide at the nanometer level. Proc Natl Acad Sci USA 2009;106(13):4975–80.

[4] Liu Z, Liu Y, Chen B, Zhu T, Ma L. Novel Fe–Ce–Ti catalyst with remarkable performance for the selective catalytic reduction of NOx by NH3. Catal Sci Technol 2016;6(17):6688–96.

[5] Liu Z, Feng X, Zhou Z, Feng Y, Li J. Ce–Sn binary oxide catalyst for the selective catalytic reduction of NOx by NH3. Appl Surf Sci 2018;428:526–33.

[6] Chen L, Yao X, Cao J, Yang F, Tang C, Dong L. Effect of Ti4+ and Sn4+ co-incorporation on the catalytic performance of CeO2–MnOx catalyst for low temperature NH3-SCR. Appl Surf Sci 2019;476:283–92.

[7] Yan L, Liu Y, Zha K, Li H, Shi L, Zhang D. Deep insight into the structure–activity relationship of Nb modified SnO2–CeO2 catalysts for low-temperature selective catalytic reduction of NO by NH3. Catal Sci Technol 2017;7(2):502–14.

[8] Lian Z, Shan W, Zhang Y, Wang M, He H. Morphology-dependent catalytic performance of NbOx/CeO2 catalysts for selective catalytic reduction of NOx with NH3. Ind Eng Chem Res 2018;57(38):12736–41.

[9] Zhou L, Zhang M, Liu C, Wang H, Zhang Y, Zang Y, et al. Synergistic effect over CeSnOx catalyst for the selective catalytic oxidation of NH3. ACS Appl Energy Mater 2022;5(11):14211–21.

[10] Yao X, Xiong Y, Zou W, Zhang L, Wu S, Dong X, et al. Correlation between the physicochemical properties and catalytic performances of CexSn1–‍xO2 mixed oxides for NO reduction by CO. Appl Catal B 2014;144:152–65.

[11] Chang H, Chen X, Li J, Ma L, Wang C, Liu C, et al. Improvement of activity and SO2 tolerance of Sn-modified MnOx–CeO2 catalysts for NH3-SCR at low temperatures. Environ Sci Technol 2013;47(10):5294–301.

[12] Zhang J, Wu Z, Liu T, Hu T, Wu Z, Ju X. XANES study on the valence transitions in cerium oxide nanoparticles. J Synchrotron Radiat 2001;8(2):531–2.

[13] Bansmann J, Abdel-Mageed AM, Chen S, Fauth C, Häring T, Kučerová G, et al. Chemical and electronic changes of the CeO2 support during CO oxidation on Au/CeO2 catalysts: time-resolved operando XAS at the Ce LIII edge. Catalysts 2019;9(10):785.

[14] Zhao S, Kang D, Liu Y, Wen Y, Xie X, Yi H, et al. Spontaneous formation of asymmetric oxygen vacancies in transition-metal-doped CeO2 nanorods with improved activity for carbonyl sulfide hydrolysis. ACS Catal 2020;10(20):11739–50.

[15] Prieur D, Bonani W, Popa K, Walter O, Kriegsman KW, Engelhard MH, et al. Size dependence of lattice parameter and electronic structure in CeO2 nanoparticles. Inorg Chem 2020;59(8):5760–7.

[16] Hu X, Chen J, Qu W, Liu R, Xu D, Ma Z, et al. Sulfur-resistant ceria-based low-temperature SCR catalysts with the non-bulk electronic states of ceria. Environ Sci Technol 2021;55(8):5435–41.

[17] Makdee A, Unwiset P, Chanapattharapol KC, Kidkhunthod P. Effects of Ce addition on the properties and photocatalytic activity of TiO2, investigated by X-ray absorption spectroscopy. Mater Chem Phys 2018;213:431–43.

[18] Toscani LM, Zimicz MG, Martins TS, Lamas DG, Larrondo SA. In situ X-ray absorption spectroscopy study of CuO–NiO/CeO2–ZrO2 oxides: redox characterization and its effect in catalytic performance for partial oxidation of methane. RSC Adv 2018;8(22):12190–203.

[19] Tiwari S, Khatun N, Rajput P, Bhattacharya D, Jha SN, Tseng CM, et al. Effect of defect states and oxygen vacancies on optical transitions due to Co2+ substitution in CeO2. Appl Phys A 2018;124(9):609.

[20] Francisco MSP, Landers R, Gushikem Y. Local order structure and surface acidity properties of a Nb2O5/SiO2 mixed oxide prepared by the sol-gel processing method. J Solid State Chem 2004;177(7):2432–9.

[21] Yoshida H, Tanaka T, Yoshida T, Funabiki T, Yoshida S. Control of the structure of niobium oxide species on silica by the equilibrium adsorption method. Catal Today 1996;28(1–2):79–89.

[22] Liu F, Asakura K, He H, Liu Y, Shan W, Shi X, et al. Influence of calcination temperature on iron titanate catalyst for the selective catalytic reduction of NOx with NH3. Catal Today 2011;164(1):520–7.

[23] Burcham L, Datka J, Wachs I. In situ vibrational spectroscopy studies of supported niobium oxide catalysts. J Phys Chem B 1999;103(29):6015–24.

[24] Nowak I, Ziolek M. Niobium compounds: preparation, characterization, and application in heterogeneous catalysis. Chem Rev 1999;99(12):3603–24.

[25] Onfroy T, Clet G, Houalla M. Correlations between acidity, surface structure, and catalytic activity of niobium oxide supported on zirconia. J Phys Chem B 2005;109(30):14588–94.

[26] Qu R, Gao X, Cen K, Li J. Relationship between structure and performance of a novel cerium–niobium binary oxide catalyst for selective catalytic reduction of NO with NH3. Appl Catal B 2013;142–143:290–7.